CTD-101K

CTD-101K is a modified anhydride cured epoxy system with excellent performance at cryogenic temperatures, and excellectn radiation resistance.  It is formulated with a very long pot life to enhance vacuum impregnation and RTM processing.  Quoted performance properties are obtained by using the following procedure for mixing and curing the system.

MATERIALS	     DESIGNATION          PARTS BY WEIGHT

RESIN:			PART A			      100.0

HARDENER:		PART B			       90.0

ACCELERATOR:		PART C			         1.5

MIXING TEMPERATURE:   40 - 60°C

MIXING PROCEDURE:  Combine the weighed components into a container equipped with heating and mechanical stirring.  Heat and stir the mixture until a clear solution at 40-60C is obtained.  Degass the mix at 27 in Hg for approximately 20 to 40 minutes until bubbles evolve infrequently from the mixture.  The system is now ready for application.

POT LIFE:

Temperature (°C)		Pot Life (Hr) 		Viscosity (Cp)

25			     145			    1300

40			       60			      400

60			       20			      100

Standard		        Accelerated

CURE:		       5 Hrs. @ 110°C	     1.5 Hrs. @ 135°C

POST CURE:	       16 Hrs. @ 125°C	             None

***MATERIAL SAFETY DATA SHEET***

COMPOSITE TECHNOLOGY DEVELOPMENT, INC.

1505 COAL CREEK DRIVE

LAFAYETTE, COLORADO 80026

EMERGENCY TELEPHONE NUMBER: (303) 664 0394

1. PRODUCT IDENTIFICATION

Trade Name and Synonyms

CTD-101K PART A

Chemical Name and/or Family or Description

Formulated liquid epoxide resin

CHEMICAL IDENTITY TRADE SECRET.  COMPOSITION WILL BE REVEALED TO A HEALTH 	PROFESSIONAL IN THE CASE OF A MEDICAL EMERGENCY.

2. COMPOSITION/INFORMATION ON INGREDIENTS

Special Health Effects - Carcinogenicity

Not a carcinogen as considered by NTP, IARC, or OSHA.

This product contains less than 50 ppm Epichlorohydrin, a substance known to be a carcinogen in 	the State of California

CHEMICAL NAME   	CAS #                RANGE %	EXPOSURE LIMITS

Epoxide Resin mixture	Trade secret	100%	OSHA PEL - Not established

OSHA STEL - Not established

ACGIH TWA - Not established

ACGIH STEL - Not established

3. HAZARDS IDENTIFICATION

Emergency Overview: Warning! Causes irritation.  May cause allergic skin reactions.

Primary Route(s) of Entry: Dermal

4. FIRST AID MEASURES

EYE	Flush eyes with water for at least 15 					min. Get medical attention if irritation occurs.

SKIN CONTACT	Wipe away excess material with dry towel. 			Wash with mild soap and plenty of water. Get 			medical attention if irritation occurs.

INHALATION	Remove to fresh air. If breathing is 					difficult, or irritation occurs, get medical 			attention.

INGESTION	Give 3-4 glasses of water.  Do not induce 			vomiting.  Get medical attention.

OVEREXPOSURE EFFECTS	May cause moderate skin and mild eye 					irritation.  May cause allergic skin reations.

MEDICAL CONDITIONS AGGRAVATED BY EXPOSURE Allergy, eczema or skin conditions

5. FIRE-FIGHTING MEASURES

FLASH POINT	> 200°F (> 93°C)

EXTINGUISHING MEDIA	CO2; dry chemical; water spray; foam 	SPECIAL FIREFIGHTING PROCEDURES 	Use self-contained breathing apparatus

FIRE AND EXPLOSION HAZARDS	Combustion products may be toxic

6. ACCIDENTAL RELEASE MEASURES

ACCIDENTAL RELEASE, BREAKAGE OR LEAK	Avoid all personal contact.  Clean with 					absorbent material. Put into closeable

containers. Flush area with water.

7. HANDLING AND STORAGE

STORAGE TEMPERATURE	Minimum handling temperature for storage.

HANDLING/STORAGE	Store in cool, dry area in closed containers.  			Avoid breathing vapor, mist or spray.  Use only 		with adequate ventilation. Eye wash and safety 			shower should be available nearby when 			product is handled.  For industrial use only.

8. EXPOSURE CONTROLS/PERSONAL PROTECTION

EYES	Chemical goggles

SKIN	Lab coats or coveralls, and impervious rubber 			gloves.  Use of barrier cream recommended.

INHALATION	Use NIOSH approved respirator suitable for 			organic vapors.

VENTILATION	General mechanical ventilation and local 			exhaust.

9. PHYSICAL AND CHEMICAL PROPERTIES

PHYSICAL FORM	Liquid

APPEARANCE AND ODOR	Clear, slight odor

BOILING  POINT	> 200°C (> 392°F)

SOLUBILITY IN WATER	Insoluble

SPECIFIC GRAVITY	~1.2g/cc

DECOMPOSITION TEMPERATURE	> 200°C (> 392°F)

10. STABILITY AND REACTIVITY

STABILITY	Stable

INCOMPATIBILITIES	Strong oxidizing agents

HAZARDOUS DECOMPOSITION PRODUCTS	Carbon monoxide, carbon dioxide and aldehydes.

HAZARDOUS POLYMERIZATION	Will not occur

CONDITIONS TO AVOID	Strong acids or bases in bulk and elevated 			temperatures

11. TOXICOLOGICAL INFORMATION

ORAL LD50 	> 5000 mg/kg - rat	DERMAL LD50	> 6000 mg/kg - rabbit

SKIN IRRITATION	Moderate irritation - rabbit

EYE IRRITATION	Slight irritation - rabbit

SENSITIZATION	Moderate sensitizer

12. ECOLOGICAL INFORMATION

Data not yet available

13. DISPOSAL CONSIDERATIONS

According  to Federal, State, and Local regulations. This product is not considered to be a 	hazardous waste by RCRA.

14. TRANSPORT INFORMATION

DEPARTMENT OF TRANSPORTATION	Not regulated

15. REGULATORY INFORMATION

OSHA STATUS	This MSDS has been prepared in compliance 			with Federal OSHA Hazard Communication 			Standard 29 CFR 1910.1200.  This product is 			considered to be a hazardous chemical under 			that standard.

RCRA	Not a hazardous waste under RCRA

(40 CFR 261)

TSCA INVENTORY STATUS	Chemical components listed on TSCA

Inventory

SARA/TITLE III:	This product does not contain a toxic

chemical under SEC. 313 (40 CFR 372)

CERLA	Not listed

CALIFORNIA PROPOSITION 65	This product contains less than 50 ppm 					Epichlorohydrin, a substance known to the State 		of California to cause cancer.

16. OTHER INFORMATION

FOR TECHNICAL INFORMATION CONTACT:	DR. NASEEM A. MUNSHI

COORDINATOR OF PRODUCT SAFETY

COMPOSITE TECHNOLOGY DEVELOPMENT,INC	ISSUE DATE: 01/05/99

1505 COAL CREEK DRIVE	REVISION DATE & NO.:

LAFAYETTE, CO 80026

(303) 664-0394

THE INFORMATION AND RECOMMENDATIONS CONTAINED HEREIN ARE BASED UPON DATA BELIEVED 	TO BE ACCURATE. HOWEVER, NO GUARANTEE OR WARRANTY OF ANY KIND EXPRESSED OR IMPLIED 	IS MADE WITH RESPECT TO THE INFORMATION CONTAINED HEREIN.

***MATERIAL SAFETY DATA SHEET***

COMPOSITE TECHNOLOGY DEVELOPMENT, INC.

1505 COAL CREEK DRIVE

LAFAYETTE, COLORADO 80026

EMERGENCY TELEPHONE NUMBER: (303) 664 0394

1. PRODUCT IDENTIFICATION

Trade Name and Synonyms

CTD-101K PART B

Chemical Name and/or Family or Description

Formulated liquid hardener

CHEMICAL IDENTITY TRADE SECRET.  COMPOSITION WILL BE REVEALED TO A HEALTH 	PROFESSIONAL IN THE CASE OF A MEDICAL EMERGENCY.

2. COMPOSITION/INFORMATION ON INGREDIENTS

Special Health Effects - Carcinogenicity

Not reviewed by NTP, IARC, or OSHA.

CHEMICAL NAME   	CAS #                RANGE %	EXPOSURE LIMITS

Methyl Nadic Anhydride	25134-21-8	Trade secret	OSHA PEL - Not established

OSHA STEL - Not established

ACGIH TWA - Not established

ACGIH STEL - Not established

3. HAZARDS IDENTIFICATION

Emergency Overview: Warning! Corrosive.  Causes skin and eye burns.  May cause allergic 	skin reactions.

Primary Route(s) of Entry: Dermal

4. FIRST AID MEASURES

EYE	Flush eyes with water for at least 15 					min. Get medical attention if irritation occurs.

SKIN CONTACT	Wipe away excess material with dry towel. 			Wash with mild soap and plenty of water. Get 			immediate medical attention.

INHALATION	Remove to fresh air. If breathing is 					difficult, or irritation occurs, get immediate 			medical attention.

INGESTION	Give 3-4 glasses of water.  Do not induce 			vomiting.  Get immediate medical attention.

OVEREXPOSURE EFFECTS	Warning! Corrosive.  Causes skin and eye burns.  		May cause allergic skin reactions.

MEDICAL CONDITIONS AGGRAVATED BY EXPOSURE Allergy, eczema or skin conditions

5. FIRE-FIGHTING MEASURES

FLASH POINT	275°F (135°C)

EXTINGUISHING MEDIA	CO2; water in copious amounts 	SPECIAL FIREFIGHTING PROCEDURES 	Use self-contained breathing apparatus

FIRE AND EXPLOSION HAZARDS	Combustion products may be toxic

6. ACCIDENTAL RELEASE MEASURES

ACCIDENTAL RELEASE, BREAKAGE OR LEAK	Remove sources of heat.  Wear protective 			equipment.  Take up with absorbent material. 			Put into closeable containers. Neutralize area 			with soda ash and water.  Flush area with water.

7. HANDLING AND STORAGE

HANDLING/STORAGE	Store away from heat, oxidizing agents and 			alkaline materials.

Corrosive.  Causes skin and eye burns. Avoid 			breathing vapor, mist or spray.  Store in cool, 			dry area in closed containers.  Use only with 			adequate ventilation. Eye wash and safety 			shower should be available nearby when 			product is handled.  For industrial use only.

8. EXPOSURE CONTROLS/PERSONAL PROTECTION

EYES	Chemical goggles

SKIN	Wear impervious rubber gloves.

INHALATION	Use NIOSH approved respirator suitable for 			organic vapors.

VENTILATION	General mechanical ventilation and local 			exhaust.

9. PHYSICAL AND CHEMICAL PROPERTIES

PHYSICAL FORM	Viscous liquid

APPEARANCE AND ODOR	Clear, light yellow

SOLUBILITY IN WATER	Reacts with water

SPECIFIC GRAVITY	~1.2g/cc

BOILING  POINT	> 250°C (> 482°F)

DECOMPOSITION TEMPERATURE	> 200°C (> 392°F)

10. STABILITY AND REACTIVITY

STABILITY	Stable

INCOMPATIBILITIES	Strong oxidizing agents, water, alkali metal 			ions, alkaline materials

HAZARDOUS DECOMPOSITION PRODUCTS	Carbon monoxide, carbon dioxide and aldehydes.

HAZARDOUS POLYMERIZATION	May occur above 200°C

CONDITIONS TO AVOID	High temperatures in the presence of alkali 			metal ions.

11. TOXICOLOGICAL INFORMATION

ORAL LD50 	~ 640 mg/kg - rat	DERMAL LD50	~ 4900 mg/kg - rat

INHALATION LC50	~ 750 mg/cu.m/4h - rat

SKIN IRRITATION	Corrosive

EYE IRRITATION	Corrosive

SENSITIZATION	Sensitizer

12. ECOLOGICAL INFORMATION

Data not yet available

13. DISPOSAL CONSIDERATIONS

According  to Federal, State, and Local regulations. This product is not considered to be a 	hazardous waste by RCRA.

14. TRANSPORT INFORMATION

PROPER SHIPPING NAME	Corrosive liquid, n.o.s. (Contains Methyl nadic			anhydride)

ID NUMBER	UN 1760

LABEL REQUIRED	Corrosive

HAZARD CLASS	8

PACKING GROUP	II

15. REGULATORY INFORMATION

OSHA STATUS	This MSDS has been prepared in compliance 			with Federal OSHA Hazard Communication 			Standard 29 CFR 1910.1200.  This product is 			considered to be a hazardous chemical under 			that standard.

RCRA	Not a hazardous waste under RCRA

(40 CFR 261), but handle with care due to 			corrosive effect on skin and eyes.

TSCA INVENTORY STATUS	Chemical components listed on TSCA Inventory

SARA/TITLE III:	This product does not contain a toxic

chemical under SEC. 313 (40 CFR 372)

CERLA	Not listed

CALIFORNIA PROPOSITION 65	This product does not contain any substance 			known to the State of California to cause cancer.

16. OTHER INFORMATION

FOR TECHNICAL INFORMATION CONTACT:	DR. NASEEM A. MUNSHI

COORDINATOR OF PRODUCT SAFETY

COMPOSITE TECHNOLOGY DEVELOPMENT,INC	ISSUE DATE: 01/05/99

1505 COAL CREEK DRIVE	REVISION DATE & NO.:

LAFAYETTE, CO 80026

(303) 664-0394

THE INFORMATION AND RECOMMENDATIONS CONTAINED HEREIN ARE BASED UPON DATA BELIEVED 	TO BE ACCURATE. HOWEVER, NO GUARANTEE OR WARRANTY OF ANY KIND EXPRESSED OR IMPLIED 	IS MADE WITH RESPECT TO THE INFORMATION CONTAINED HEREIN.

***MATERIAL SAFETY DATA SHEET***

COMPOSITE TECHNOLOGY DEVELOPMENT, INC.

1505 COAL CREEK DRIVE

LAFAYETTE, COLORADO 80026

EMERGENCY TELEPHONE NUMBER: (303) 664 0394

1. PRODUCT IDENTIFICATION

Trade Name and Synonyms

CTD-101K PART C

Chemical Name and/or Family or Description

Accelerator for curing epoxy resins

CHEMICAL IDENTITY TRADE SECRET.  COMPOSITION WILL BE REVEALED TO A HEALTH 	PROFESSIONAL IN THE CASE OF A MEDICAL EMERGENCY.

2. COMPOSITION/INFORMATION ON INGREDIENTS

Carcinogenicity: Not reviewed by OSHA, IARC or NTP

CHEMICAL NAME   	CAS #     	RANGE %	EXPOSURE LIMITS

Dibutyl Phthalate	84-74-2	Trade secret	OSHA PEL - 5 mg/m3

ACGIH TWA - 5 mg/m3

Phenol	108-95-2	Trade secret	OSHA PEL - 5 ppm

ACGIH TWA - 5 ppm

3. HAZARDS IDENTIFICATION

Emergency Overview: Severely irritating to eyes, nose and throat.  Prolonged overexposure 	may cause collapse and liver or kidney damage.  May cause allergic skin reactions.

Primary Route(s) of Entry: Dermal

4. FIRST AID MEASURES

EYE	Flush eyes with water for at least 15 					min. Get medical attention if irritation occurs.

SKIN CONTACT	Wipe away excess material with dry towel. 			Wash with mild soap and plenty of water. Get 			immediate medical attention.

INHALATION	Remove to fresh air. If breathing is 					difficult, or irritation occurs, get immediate 			medical attention.

INGESTION	Give 3-4 glasses of water.  Do not induce 			vomiting.  Get immediate medical attention.

OVEREXPOSURE EFFECTS	Overexposure may produce weakness, 					.headache, dizzinesss.  Prolonged overexposure 			may cause collapse and liver or kidney damage

MEDICAL CONDITIONS AGGRAVATED BY EXPOSURE Allergy, eczema or skin conditions

5. FIRE-FIGHTING MEASURES

FLASH POINT	180°F (82°C)

EXTINGUISHING MEDIA	CO2; water spray, dry chemical, foam 	SPECIAL FIREFIGHTING PROCEDURES 	Use self-contained breathing apparatus

FIRE AND EXPLOSION HAZARDS	Combustion products may be toxic

6. ACCIDENTAL RELEASE MEASURES

ACCIDENTAL RELEASE, BREAKAGE OR LEAK	Avoid all personal contact.  Wear protective 			equipment.  Take up with absorbent material. Put 		into closeable containers. Flush area with water.

7. HANDLING AND STORAGE

HANDLING/STORAGE	Store away from heat, oxidizing agents and 			alkaline materials.

Causes severe skin and eye irritation. Avoid 			breathing vapor, mist or spray.  Store in cool, 			dry area in closed containers.  Use only with 			adequate ventilation. Eye wash and safety 			shower should be available nearby when 			product is handled.  For industrial use only.

8. EXPOSURE CONTROLS/PERSONAL PROTECTION

EYES	Chemical goggles

SKIN	Wear impervious rubber gloves.

INHALATION	Use NIOSH approved respirator suitable for 			organic vapors.

VENTILATION	General mechanical ventilation and local 			exhaust.

9. PHYSICAL AND CHEMICAL PROPERTIES

PHYSICAL FORM	Liquid

APPEARANCE AND ODOR	Clear, amine odor

SOLUBILITY IN WATER	Soluble

SPECIFIC GRAVITY	~1.0g/cc

BOILING  POINT	> 150°C (> 302°F)

DECOMPOSITION TEMPERATURE	> 200°C (> 392°F)

10. STABILITY AND REACTIVITY

STABILITY	Stable

INCOMPATIBILITIES	Strong oxidizing agents, strong acids, and 			strong alkaline materials

HAZARDOUS DECOMPOSITION PRODUCTS	Carbon monoxide, carbon dioxide, aldehydes, 			and nitrogen oxides

HAZARDOUS POLYMERIZATION	Will not occur

CONDITIONS TO AVOID	High temperatures.

11. TOXICOLOGICAL INFORMATION

ORAL LD50 	780 mg/kg - rat	DERMAL LD50	250 mg/kg - rabbit

INHALATION LC50	> 1.06 mg/l air, 4h exposure - rat

SKIN IRRITATION	Mild - rabbit

EYE IRRITATION	Severe

SENSITIZATION	Sensitizer

12. ECOLOGICAL INFORMATION

Data not yet available.

This product contains a marine pollutant, dibutyl phthalate

13. DISPOSAL CONSIDERATIONS

According  to Federal, State, and Local regulations.

14. TRANSPORT INFORMATION

PROPER SHIPPING NAME	Environmentally hazardous substance, liquid, n.o.s. 		(Contains Dibutyl Phthalate)

ID NUMBER	UN 3082

LABEL REQUIRED	Corrosive

HAZARD CLASS	9

PACKING GROUP	III

15. REGULATORY INFORMATION

OSHA STATUS	This MSDS has been prepared in compliance 			with Federal OSHA Hazard Communication 			Standard 29 CFR 1910.1200.  This product is 			considered to be a hazardous chemical under 			that standard.

RCRA	Not a hazardous waste under RCRA (40 CFR 			261)

TSCA INVENTORY STATUS	Chemical components listed on TSCA Inventory

TSCA 12(b) EXPORT NOTIFICATION	This product contains chemical(s) which are 			regulated by TSCA 12(b) Regulation and it is 			required that proper export notification shall be 		sent to EPA prior to shipping out of the US.

SARA/TITLE III:	This product contains a toxic chemical under 			SEC. 313 (40 CFR 372): 50%; 84-74-2; 			Dibutyl Phthalate, & 16.8%; 108-95-2, Phenol

CERLA	RQ 20lb (Dibutyl Phthalate) (U069)

CALIFORNIA PROPOSITION 65	This product does not contain any substance 			known to the State of California to cause cancer.

16. OTHER INFORMATION

FOR TECHNICAL INFORMATION CONTACT:	DR. NASEEM A. MUNSHI

COORDINATOR OF PRODUCT SAFETY

COMPOSITE TECHNOLOGY DEVELOPMENT,INC	ISSUE DATE: 01/05/99

1505 COAL CREEK DRIVE	REVISION DATE & NO.:

LAFAYETTE, CO 80026

(303) 664-0394

THE INFORMATION AND RECOMMENDATIONS CONTAINED HEREIN ARE BASED UPON DATA BELIEVED 	TO BE ACCURATE. HOWEVER, NO GUARANTEE OR WARRANTY OF ANY KIND EXPRESSED OR IMPLIED 	IS MADE WITH RESPECT TO THE INFORMATION CONTAINED HEREIN.