# Text boxes

Epoxy Mix Tank

Vac. pump

Resin & Accelerator

Hardener

Epoxy manifold

Epoxy Overfill Manifold

Autoclave

Epoxy Overfill Manifold

Vacuum Manifold

Heating jacket

Heating jacket

Vacuum Manifold

N2

Vent

Vent

(15) Feedthru’s (typical 2 locations)

Relief Valve

Relief Valve

# Poly-flo tubing

High temperature vacuum tubing

(20-30)

VPI Sprues

Drain valve

Autoclave:

- Heating to 135 degrees C

- Max. Pressure 10 psig

- Vacuum to mTorr range

Vent

Drain valve

NCSX Modular Coil VPI Flow Diagram

12/17/02        J.H. Chrzanowski