| Princeton Plasma Physics Laboratory Procedure |
| --- |
| ‘ Procedure Title: General Silver Plating Procedure |
| Number: D-NSTX/NCSX-IP-2853 | Revision: 01 | Effective Date: Expiration Date: (2 yrs. unless otherwise stipulated) |
| Procedure Approvals |
| Author: James H. Chrzanowski | Date: |
| ATI: James H. Chrzanowski | Date: |
| RLM: Al vonHalle | Date: |
| Responsible Division: NSTX and NCSX Projects |
| Procedure Requirements Designated by RLM LABWIDE: |
|  | Work Planning Form # W__ (ENG-032) |  | Lockout/Tagout (ESH-016) |
|  | Confined Space Permit (5008,SEC.8 Chap 5) |  | Lift Procedure (ENG-021) |
|  | Master Equip. List Mod (GEN-005) | X | ES&H Review (NEPA, IH, etc.) NEPA 1292 |
|  | RWP (HP-OP-20) |  | Independent Review |
|  | ATI Walkdown | X | Pre-Job Brief |
|  | Post-job Brief * |  |  |
| D-SITE SPECIFIC: |
| X | D-Site Work Permit (OP-AD-09) |  | Door Permit (OP-G-93) |
|  | Tritium Work Permit (OP-AD-49) |  | USQD (OP-AD-63) |
| X | Pre-Job Brief (OP-AD-79) |  | T-Mod (OP-AD-03) |
|  | ** DCA/DCN (OP-AD-104) # |  |  |

*  Required for installations involving internal vacuum installations, critical lifts, and for the initial installation of repetitive work.

** 	OP-AD-104 was voided by procedure ENG-032. However, DCAs that were open at the time of adoption of ENG-032 are still considered valid for work approval purposes.

REVIEWERS (designated by RLM) Rec’d/ Incorp. Comments

Accountable Technical Individual. …………J. Chrzanowski

Test Director

Independent Reviewer

D-Site Shift Supervisor

NCSX ………………………………………………………….Tom Meighan X

Vacuum

NSTX ………………………………………………………..Joe Winston X

Quality Assurance/Quality Control. …………………………

Maintenance and Operations Division

Energy Conversion System/Motor Control Division

Engineering …………………………………….. …………………………….Erik Perry X

Environmental Restoration & Waste Management Division

Environmental, Safety & Health……………………………………………………Jerry Levine X

Industrial Hygiene………………………………………………... Bill Slavin X

Health Physics…………………

RLM ………………………………………………………………..Al vonHalle

| TRAINING (designated by RLM) |
| --- |
| No training required ______________ | Instructor Jim Chrzanowski |
| Personnel (group, job title or individual name) | Read Only | Instruction Pre-job Briefing | Hands On |
| Lead Tech. |  | X |  |
| Technicians performing task |  | X |  |
| Field Supervisors |  |  |  |
| Quality Control Representative |  |  |  |
| Training Rep. |
| RLM Al vonHalle |

RECORD OF CHANGE

| Revision | Date | Description of Change |
| --- | --- | --- |
| 00 | 10/23/03 | Initial release |
| 01 | 1/2/07 | Procedure expanded to include NCSX and NSTX projects 7.11 Changed the identification of Hazardous waste storage |

1.0	PURPOSE:

## The purpose of this document is to provide a general silver-plating procedure for the NCSX and NSTX activities. It describes the process for silver-plating copper surfaces with the use of a Portable Silver-Plating Unit, and includes the safety precautions to be taken when silver-plating copper electrical surfaces.

- SCOPE:

This procedure will describe the following processes:

  - Preparation of the electrical contact faces prior to silver-plating

  - Safety precautions and prerequisites associated with silver-plating.

  - Process steps for silver-plating

Note:  Cognizant Individual is defined in this procedure to be the individual requesting that the silver-plating process be performed or the owner of the material being plated.

3.0	REFERENCE DOCUMENTS:

  - ESHD-5008, Environmental, Safety and Health Manual

  - MSDS….. Rapid Electroplating No. 316 Silver Coatalyte

- PREREQUISITIES:

  - A JHA MUST be generated and reviewed everytime this procedure is used

JHA complete: Verification by Cognizant Individual _______________ Date: ____________

  - The plating area must be well exhaust ventilated.

  - Goggles and butyl or neoprene rubber gloves must be worn during the plating process.

  - Avoid skin contact with the silver-plating solutions.

  - Face shields and rubber apron should be used if needed to prevent contact.

  - A Pre-job briefing must be completed prior to starting this procedure.  Provisions of all safety related issues via the Job Hazard Analysis sheets must be reviewed at this meeting.

###### Pre-Job Briefing Complete Date: _____________ Performed By: ___________________

  - Obtain a D-site Work Permit for all work performed at D-site.

###### D-Site Work Permit: ________________________

- MATERIALS AND SPECIAL EQUIPMENT

  - Materials & Equipment:

    - Rapid- Portable Plating Unit

    - Silver applicator wand

    - Silver coatalyte #316

    - Scotch-brite pads

    - Degreaser

- Preparation of Surfaces to be Plated:

  - Thoroughly clean (degrease) the area that is to be silver-plated; using IH approved cleaning solvents and scotchbrite pads.  Use appropriate hand and eye protection during this process.

    - Clean the surface to be plated with the “Green” scotchbrite pad to remove any oxidation.

    - Wipe the area with a clean cloth and wipe down the area again with a clean cloth and ethanol.

    - Silver plate as soon as the ethanol has dried.

- Silver Plating Process:

  - Plug the silver-plating power unit into a 110/120 volt 50/60 HZ circuit.

  - Connect the black lead to the negative (-) terminal and the red lead to the (+) terminal of the plater.

  - Connect the black lead to the surface being silver-plated.  Plug the red lead into the applicator.

  - Turn the switch to “ON” and adjust the voltage to 10 volts.  Turn switch “OFF” until ready to plate (Ammeter should show no readings accept when plating).

  - Turn on the plater; the meter should read 10 volts.  If not, adjust the controller until it does.

  - Dip the silver applicator into the Silver Coatalyte #316 and begin plating with short circular or forward and backward rubbing actions; dipping the applicator in the coatalyte at intervals.

  - Continue plating until the entire surface is covered.

  - After plating, rinse the work off with water and wipe dry with cotton rags.

  - Lightly buff the silver-plated area with a white Scotchbrite pad.

  - Ensure that there are no traces of the silver-plating solution left behind.

  - Place all waste in an approved Hazmat satellite container, and notify Hazmat for pick-up.

  - The final plating surfaces should be inspected and approved by the Cognizant individual requesting the plating operation.

8.0  	COMPLETION SIGNOFF:

  - This procedure has been completed per the requirements and steps outlined in this procedure.

###### Cognizant Individuals verification: __________________________________ Date: ____________

COMMENTS: