#### NCSX

# Modular Coil

Lead Braze Development Program Preliminary Results

September 16, 2004

By James H. Chrzanowski

Several specimens for fabricated and tested for developing the techniques of terminating the modular coil leads.  The copper termination leads are as shown in the figure 1 below.

Added braze feed hole to terminal (#49 drill size) 0.073 inch diameter

The compacted copper conductor was brazed into the lead termination blocks using Sil-Fos braze material.  A Nibco carbon tong heating unit was utilitized for heating the specimen to the braze temperature.

The Sil-Fos was fed through the feed-hole        Back feeding from the cable end

## Figure 4                                                             Figure 5

Finished braze operations- Figure 6

Specimen dissected –Figure 7

Specimen dissected- Figure 8

An additional specimen was fabricated with a lead termination on each end of the cable.  The specimen was then pulled in the tensile tester. The cable joint broke at a load of 2300# adjacent to the braze joint in the heat affected zone.  (See figures 9 and 10)

Figure 9

Figure 10

# Text boxes

The copper conductor was first rounded using phenolic form blocks to provide a proper fit between the cable and terminal block.

## Figure 2

A chill block provided the necessary cooling to protect the copper conductor from the advancing heat.

The carbon tongs were positioned over the solid part of the termination block

## Figure 3

Figure 1