| 4.2.1 Vacuum Test | Thermally cycled (375 C), three times. |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 4.2.2 Surface Finish | profilometer to verify compliance with Section 3.2.2. | Sub:4 Op#:10 Sub:162 Op#:20 Sub:167 Op#:10 Sub:168 Op#:10 Sub:163 Op#:20 Sub:172 Op#:10 Sub:173 Op#:10 Sub:5 Op#:10 Sub 164 Op#10 And many more |  |  |  |  |  |
| 4.2.3 Verification of Magnetic Permeability | verify conformance to Section 3.2.4, 6" x 6" grid. weld seams shall be checked every 1/2" | On receipt as in Subs 248 & 249, Op#10, for example After forming as in steps like Sub 26 Op#30 |  |  |  |  |  |
| 4.2.4 Verification of Dimensions and Tolerances | grid no coarser than 1-inch centers Welds seams and each end of the Period Assembly and Spacer shall be dimensionally checked on 1 inch centers. |  |  |  |  |  |  |
| 4.2.5 Material certifications | a. N06625: showing actual chemical and physical properties b. Bolts: Manufacturer’s certification of grade c. Conflat flanges: Manufacturer’s certification of grade d. Filler metal: showing actual chemical properties |  |  |  |  |  |  |
| 4.2.6.1 Visual | 8X magnification. AWS D1.6, par. 6.29.1 |  |  |  |  |  |  |
| 4.2.6.2 RT | 10% of each seam ASME UW-51 |  |  |  |  |  |  |
| 4.2.7 Cleaning |  |  |  |  |  |  |  |