Review of the FEA and Testing Results for the 18-Turn Beam

Introduction

The measured modular coil deflections for flexural test of the 18-turn straight beam [1] are much higher than the FEA results that were computed on the basis of assumed material properties [2].  The test data are the measured values from the actual beam deflections and the FEA results are calculated from the sound analytical theory.  They should be very close if the measurements and the analytical assumptions were doing correctly.

Possible errors

To find out the discrepancy between the analytical and the test results, the following three areas will be examined:

A) The possible errors of the finite element model are from the assumed material properties and the beam shape.  Here are the FEA input data [2]:

- Conductor is 0.500 x 0.625 inches

- Turn insulation is 0.03 inches

- Ground wrap is 0.03 inches

- E of conductor is 9.5E6 psi

- E of turn insulation is 1.5E6 psi

- E of ground wrap is 1.5E6 psi

- Poissons’ ratio is 0.31

The FEA model consists of conductors, turn insulations, and ground wrap.  In the analysis, the material properties were assumed to be isotropic and the displacements are mainly determined by the assumed modulus values.  Are the assumed values of material properties correct?  Does the assumption of isotropic material property produce reasonable results?

B) The possible errors from the test are the accuracy of test instruments, the testing arrangement, and the reading and interpretation of the measured data.  Do the load, extensometer, and reading instruments calibrated before the testing?  Do any additional deformations due to the test setup exist during the test?  What is the degree of accuracy of the instrument reading with respect to the actual deformation?

C) The another possibility is the precision of the test specimen.  Are the beam dimensions and VPI process flawless?  Does the beam have perfect bonding between components so that no nonlinear effects such as surface sliding occur during the test?

Discussions

1) Beam Shape and Conductor Material property

The total depth of beam modelled in the FEA is 5.1”, which is smaller than the actual beam height of 5.58”.  The lower depth in beam shall predict a higher deflection, not the smaller deflection.   Since the isotropic material properties were utilized in the analysis, the shear modulus was automatically determined by the assumed Poissons’ ratio.  A series of tests has been conducted by the Composite Technology Development, Inc. in 2003 [3] for the resin impregnated single conductor that comprised of four 0.3125” by 0.250” braided copper and wound with glass/kapton turn insulation.  The test results were summarized in a report by Zatz [4] showing the dissimilarity in the elastic moduli due to axial compression, axial tension, and flexural bending.  The standard deviations in the same group of test results are found to be large.   The moduli also varied with the testing temperature but inconsistency in the trend with respect to the temperature ranges.  Table 1 shows the modulus of elasticity caused by different loading conditions at the elected temperature of 150°K.

Table 1: Modulus of Coil Conductor at 150°K

Loading		   Temperature(K)	  	   Modulus(Mpsi)

Axial Compression		150				7.9

Axial Tension		150				14.1

Flexural (Flatwise)	150				4.3

Flexural (Edgewise)	150				4.1

The flexural moduli were tested following ASTM D790 in a three-point bending configuration.  The specimens were tested in two different directions designated as “flatwise”, which has bending about its weaker axis with a depth/span ratio of 12.3, and “edgewise”, which has bending about its stiffer axis with a depth/span ratio of 10.3.  The flexural modulus that involved the combining effects of axial modulus and shear modulus was calculated from the following equation [3], an equivalent modulus for bending moment:

EB=L3m/4 bd3

Where:

EB = modulus of elasticity in bending

L = support span

b = width of specimen

d = depth of specimen

m = slope of the tangent to the initial straight-line portion of 		    		the load-deflection curve

In view of the less lateral stiffness under the axial compression due to the twisted copper strands, the tension modulus was expected to be larger than the compression modulus.  For similar reason, the conductor is stiffer in the axial direction and softer in the transverse direction.  If the beam is not too long, the deflection of beam will be produced by the bending moment and by the shear force, in the form of a mutual sliding of adjacent cross sections along each other.  A better way of making the FEA model is to employ the orthotropic material property, from which a more accurate shear modulus can be entered for the conductor.  Even with the orthotropic material property, it is still not able to simulate the actual property of the modular coil because of the dissimilarity material properties in the axial tension and the axial compression.

2) Shear modulus in the Conductor

Lower modulus in the flexural test indicated the effect of shear deformation, which is caused by the shear modulus G of the composite modular coil.  Because of the composite action in the modular coil, the shear modulus of conductor is considered to be smaller than the shear modulus of the solid copper conductor.  The use of axial modulus as the isotropic elastic modulus will overestimate the stiffness of beam due to underestimate the shear deformation in the flexural analysis.

The short beam flexural tests (depth/span ratio of about 5.0) for the 2x2 modular coil bundles [3] revealed even smaller flexural moduli that ranged from 2.3 Mpsi at 76°K to 1.1 Mpsi at 295°K.  The results pointed out that the shear modulus will be small at the room temperature.  The conclusion was further proved by the plug longitudinal shear tests [5] of short conductor specimens that showed a very small average shear modulus of 0.139 Mpsi at the room temperature.

3) FEA Runs for Some Selected Material Properties

Assuming that the modulus of elasticity is 1.5 Mpsi and a Poisson’s ratio is 0.31 for the turn insulation and ground wrap, four FEA runs were selected in Table 2 to test the variations of conductor material properties due to 4000 pounds of center load.

Table 2: Material Property Selected for FEA Runs

The FEA model and results of Run No.1 has been documented in the previous report [2]. In the rectangular coordinate system, y-axis is in the vertical direction and z-axis is in the longitudinal direction of the beam.  Nuxy is the minor Poissons’ ratio in ANSYS.  The use of constant shear modulus G intends to simplify the parameters since the vertical shear deformation is primarily determined by the shear modulus Gyz.  A 4000 lb concentrated load was applied on top of the beam at the mid-span within an one inch area.  Table 3 illustrates the maximum vertical deflections at the mid-span, quarter span, and the maximum/minimum axial stresses in the conductor.    The stresses in the insulation were lower because of lower modulus.

Table 3: Vertical Displacements and Max./Min. Axial Stresses

Comparing the material input and the resulting structural response, several remarks may be drawn as follows:

- Lowering shear modulus will increase both the vertical deformations and the axial stresses (comparing Runs #1 and #2)

- Lowering elastic modulus will increase the vertical deformations but decrease the axial stresses in a less fraction (comparing Runs #2 and #3

- Lower elastic modulus that perpendicular to the longitudinal direction will have negligible effects on the vertical deformations and the axial stresses (comparing Runs #2 and #4)

4) FEA Runs for Smeared Material Property

If the smeared material properties will be utilized for the analysis of the modular coil, it will need the equivalent material properties E and G for the modular coil model.  Four more ANSYS runs were carried out using the identical material property for all components as shown in Table 4.  The isotropic material property of the equivalent E in Run #5 was adopted from the calculated value in the test report [1], based on the central deflection of 0.11” and a central load of 5000 lb.  The 3.04 Mpsi equivalent E was calculated by considering only the action of bending moment that caused the deflection.

Table 4: Smeared Material Property Selected for all Components

Table 5 illustrates the maximum vertical deflections and the maximum/minimum axial stresses for FEA runs #5 through #8, under a central loading of 4000 lb.  The change of stresses and deflections has the similar trend as described in the previous section.  The FEA results will be used to compare with the simple theoretical equations in the next section.

For comparing purpose, the deflections of test results are also given here.  The actual readings of the beam deflections for 5000 lb central load are 0.1281” at the center and 0.0705” and 0.0749” (average 0.0727”) at the quarter points.  By linear interpolation into 4000 lb load, the vertical deflections become 0.1025” and 0.0582” at center and quarter point, respectively.

Table 5: Vertical Displacements and Axial Stresses for Modular Coil with Smeared Material Properties

5) Comparison with Theoretical Deflections of Smeared Beam

The deflection expression at the center point and the quarter point are given in Table 6.  For a central loading beam, the deflection equation due to bending moment is a cubic function of the distance measuring from the end support.  But the deflection equation due to shear force is a linear function of the distance measuring from the end support.  The equations of the shear deflection are derived from the conjugate beam approach [6].  In the shear equation,  is a numerical factor, with which the average shearing stress must be multiplied in order to obtain the shearing stress at the centroid of the cross section.  For a rectangular cross section, the factor is 1.5.  As a result of the non-uniform distribution of the shear stresses, the cross sections due to the shear force do not remain as a plane.

Table 6: Deflection Equations of Simply supported Beam Due to 	Concentrated Central Load

The hand calculated deflections due to bending moment and shear force are used to compare with the FEA deflections in Table 7.  It demonstrates the increasing effects of shear deformation on the total deflection when the shear modulus is getting smaller.  The percentage of variation between hand calculated deflections and FEA results are increasing as the ratio of E/G increases.  For a very low shear rigidity, the FEA may predict a better answer since the simple equations in Table 6 neglects the Poissons’ ratio effects of the material property and the deformations in the cross sections do not stay in a plane when shear deformation is involved.

If the theoretical deflection was set to equal the FEA deflection in the Run #7, where the shear modulus is the smallest at 0.14 Mpsi, the shear deflection should be reduced to 0.0460”.  The  value should be multiplied by a factor of 0.782, which is the ratio of 0.0460/0.0588, or the shear modulus G should be divided by the factor of 0.782.  Similarly for the Run #8, the factor will be 0.0776, which is the ratio of 0.0456/0.0588.

Table 7: Comparison of the Calculated and FEA Deflections

Theoretical Def. at center       FEA Def.		Theoretical Def. at ¼ Span     FEA Def.

| Run No. | Due to Bending | Due to Shear | Total | Vertical Def. At Center | Diff. | Due to Bending | Due to Shear | Total | Vertical Def. At 1/4 span | Diff. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (in) | (in) | (in) | (in) | (%) | (in) | (in) | (in) | (in) | (%) |
| 5 | 0.1110 | 0.0071 | 0.1181 | 0.1172 | 0.7 | 0.0763 | 0.0035 | 0.0798 | 0.0800 | -0.2 |
| 6 | 0.0536 | 0.0165 | 0.0700 | 0.0670 | 4.5 | 0.0368 | 0.0082 | 0.0450 | 0.0440 | 2.3 |
| 7 | 0.0536 | 0.0588 | 0.1123 | 0.0996 | 12.8 | 0.0368 | 0.0294 | 0.0662 | 0.0611 | 8.3 |
| 8 | 0.0355 | 0.0588 | 0.0943 | 0.0811 | 16.3 | 0.0244 | 0.0294 | 0.0538 | 0.0484 | 11.2 |

6) Evaluating Material Properties from the Test Data

The deflection equation in Table 6 may be used to predict the elastic moduli E and G for the testing beam.  Since the total beam deflection is the superposition of deflections due to bending moment and shear force, the deflection equations for the mid-span and the ¼ span become:

At the mid-span:	 = PL3/48EI + PL/4AG

At the ¼ span:	 = 11PL3/768EI + PL/8AG

The above equations have two unknown variables and the beam testing also provides deflections at the corresponding locations.  They are 0.1281” at the center and 0.0705” and 0.0749” (average 0.0727”) at the quarter points for a 5000 lb central load.  Substituting the loading, beam span, and sectional properties, the equations become:

0.1281 = 421740/E + 10284/G

0.0727 = 289950/E + 5142/G

Solving the above two equations results the equivalent moduli as:

E = 9.142 Mpsi

G = 0.126 Mpsi

As the ratio equivalent E/G is large, It may be more accurate to modify the above equations by replacing the G into G/0.776.  The two equations are solved again and the new modulus of elasticity becomes:

E = 9.142 Mpsi

G = 0.0983 Mpsi

To check the appraised values of the equivalent E and G values, the appraised values were used as input for the FEA model to evaluate and compare the beam deflections.  A concentrated load of 5000 lb was applied at beam center.  Table 8 shows the smeared material input.  The FEA results for stresses and deflections are summarized in Table 9.  Close agreement within 1.8% difference was obtained between the test results and the FEA results based on the calculated equivalent E and G for the Run #10.

Table 8: Smeared Material Property Selected for all Components

Table 9: Vertical Displacements and Axial Stresses for Modular Coil with Smeared Material Properties

Although good concurrence was found in the deflection, the level of the maximum stress may be high enough to cause the nonlinear load-deformation relationship.  The simple deflection equations for bending moment and shear force are established from the linear stress-strain curves.  It will be a good verification to derive the equivalent moduli by picking up the test deflections at another load level.

[TBD]

7) Experiment Setup and Instruments Calibrations

[TBD]

It is assumed that all the testing instruments have been calibrated in the reading before the test.

The test beam was held at ends of beam by clevis loading frames which were supported by hanging rods and W12x26 WF beam on the top.  The LVDTs were mounted between the LVDT support and the beam specimen at 5 locations to measure the deformation.  It shows that at the maximum stroke of 0.2011” with maximum load of 4994.8 lb, the LVDT readings at supports are about 0.04”, which could be caused by the displacements of hanger rods and top WF-beam.  The deflections of beam have been corrected to eliminate the effects of the end deformation.

It is important that the position of LVDT keeps on the same level.  If the LVDT are mounted on the clevis loading frames, the additional deformation due to the clevis loading frames should be taken in to consideration.

8) Experiment Reading

[TBD]

The following readings show the actual deflection may have reading error of about 0.006” (0.0468-0.0412)

stroke	load		actual red	actual white

[in]		[lb]		deflection	deflection

0.135345	3198.85	0.0433	0.0475

0.135345	3200.07	0.0468	0.0454

0.135345	3202.82	0.0412	0.0479

9) Test Specimen

[TBD]

The two measured deflections on the quarter points of the beam are not identical.  At 5000 lb load, the deflections are 0.0705” at the left-hand side and 0.0749” at the right-hand side.  Is the beam uniform along the length?

At a certain load level, the deflections measured during loading and unloading stages are not equal.  It indicates either a nonlinear elastic material or, the worst case, a surface slipping inside the beam.  It may also caused by the test setup.

Conclusions

[TBD]

Orthotropic material property should be used for the conductor

Strain gage measurement may be added to read the stress of beam

References

[1] “9nov04 beam test results.xls”, Brad Nelson’s email attachment,  11/9/2004

[2] Fan, H.M.., “Finite Element Analysis of the 18 Turn Beam”, email attachment, 11/5/2004

[3] Fabian, Paul E., Test Program to Determine the Mechanical and Thermal Properties of the Epoxy/Insulation System for the NCSX Modular Ciols, Subcontract S-04353-G Report, 11/21/2003

[4] Zatz, I., “Interim NCSX Modular Coil Material Properties and Allowables”, NCSX R&D  Reports, 031212_MatProps_140_IJZ, 12/12/2003

[5] Kozub, T., NCSX Composite Coil Testing, NCSX Engineering R & D Results, 3/22/2004

[6] Timoshenko, S., “Strength of Materials, Part 1”, Third Edition, 19555