Art Brooks has suggested an approach that can avoid the deflection equations and evaluate the smeared material property.  The method is straightforward and illustrated as follows:

- Run several beam cases with variable E and G values.

- Evaluate the deflections at center and quarter span locations and plot the relationship between the E/G ratios and deflection ratios as below.

- Calculate deflection ratio from the beam test results

Ratio = 0.1283” / 0.0736” = 1.743

- Fit the deflection ratio 1.743 into the curve to estimate the E/G ratio, which is about 133.

- Use the E value of 13.3 Mpsi and G value of 0.1 Mpsi in a FEA run.  The analysis give a center deflection of  0.10996”

- Because of the linear theory, the actual material properties can be estimated by

E = 13.3 x (0.10996/0.1283) = 11.399 Mpas

G = 0.10 x (0.10996/0.1283) = 0.857 Mpsi