| NATIONAL COMPACT STELLARATOR PROJECT Engineering Change Proposal (ECP) |
| --- |
| COVER PAGE (TO BE COMPLETED BY SYSTEMS ENGINEERING SUPPORT MANAGER) |
| Originator: Bob Simmons | Date: February 16, 2005 |
| ECP No: 023 | ECP Title: Charpy V-Notch Requirements |
| Required Reviewers |
| Required Reviewers for this ECP: P. Hietzenroeder, Brad Nelson, Dave Williamson |
| ECP Approval Level Expedited ECP? Yes No Change Level: Approving Official: |
| Actions Revise MCWF CSPEC (NCSX-CSPEC-141-03) by March 31, 2005 to reflect revised Table 3-2. |
| APPROVALS (TO BE COMPLETED BY APPROVING OFFICIALS) |
| Change Level | Approving Official | Approval? | Signature |
| 3 | NCSX Project Manager | Yes No |  |
| 3a (Expedited ECP) | NCSX Engineering Manager | Yes No |  |
| 2 | NCSX Federal Project Director | Yes No |  |
| 1 | Associate Director OFES | Yes No |  |
| 0 | Under Secretary of Energy | Yes No |  |

| NATIONAL COMPACT STELLARATOR PROJECT Engineering Change Proposal (ECP) |
| --- |
| PART I (TO BE COMPLETED BY ORIGINATOR) |
| Originator: Bob Simmons | Date: February 16, 2005 |
| Overview of Change Type of of ECP: EXPEDITED STANDARD Type of Change: TECHNICAL COST SCHEDULE EDITORIAL (Check all that Apply) Reason for Change: We did not have impact testing requirements for the weld material during the prototype phase, and consequently testing of this was not done. While reviewing the weld procedures and qualification material for welding, it was noted that we did not have data for the weld. MetalTek sent the supplier’s data, and it is lower than we specify (50J vs. 61 J). Impacted WBS Elements: WBS 141 Impacts of Change (Briefly Describe): Revise Table 3-2 (Minimum Mechanical Properties) in CSPEC to: Temperature 77K 293K Elastic Modulus 21 Msi (144.8 Gpa) 20 Msi (137.9 Gpa) 0.2% Yield Strength 72 ksi (496.4 Gpa) 34 ksi (234.4 Gpa) Tensile Strength 95 ksi (655 Gpa) 78 ksi (537.8 Gpa) Elongation 32% 36% Charpy V – notch Energy 35 ft. lbs. (47.4 J) 50 ft-lbs (67.8 J) Note: Charpy V-Notch energies were formerly 45 ft. lbs (61.0 J) for 77K and 60 ft lbs (81.3 J) for 293K. Those V-notch values were the values MetalTek was willing to guarantee for the casting alloy, based on their testing of the actual casting alloy. The welding alloy is a different chemical composition than the casting alloy, chosen to give it good welding properties. The tradeoff is that biasing the alloy to give it good welding properties results in lower V-notch values. The v-notch value is not a "typical" material property value that's used in engineering calculations - it's an indicator of the lack of brittleness of a material. The original casting V-notch values were very conservative, so accepting a lower value is considered acceptable. Assessment of Other Options: None Attachment: NCSX-CSPEC-141-07-dA |