| Princeton Plasma Physics Laboratory Procedure |
| --- |
| ‘ Procedure Title: Modular Coil Fabrication-Winding Form Preparation Activities |
| Number: D-NCSX-MCF-001-00-dA | Revision: Draft A | Effective Date: Expiration Date: (2 yrs. unless otherwise stipulated) |
| Procedure Approvals |
| Author: James H. Chrzanowski | Date: |
| ATI: James H. Chrzanowski | Date: |
| RLM: Larry Dudek | Date: |
| Responsible Division: NCSX Project |
| Procedure Requirements Designated by RLM LABWIDE: |
| X | Work Planning Form # WP-1188 & 1138 (ENG-032) |  | Lockout/Tagout (ESH-016) |
|  | Confined Space Permit (5008,SEC.8 Chap 5) |  | Lift Procedure (ENG-021) |
|  | Master Equip. List Mod (GEN-005) | X | ES&H Review (NEPA, IH, etc.) NEPA 1283 |
|  | RWP (HP-OP-20) |  | Independent Review |
|  | ATI Walkdown | X | Pre-Job Brief |
| X | Post-job Brief * |  |  |
| D-SITE SPECIFIC: |
| X | D-Site Work Permit (OP-AD-09) |  | Door Permit (OP-G-93) |
|  | Tritium Work Permit (OP-AD-49) |  | USQD (OP-AD-63) |
| X | Pre-Job Brief (OP-AD-79) |  | T-Mod (OP-AD-03) |
|  | ** DCA/DCN (OP-AD-104) # |  |  |

* Required for installations involving internal vacuum installations, critical lifts, and for the initial installation of repetitive work.

** 	OP-AD-104 was voided by procedure ENG-032. However, DCA’s that were open at the time of adoption of ENG-032 are still considered valid for work approval purposes.

REVIEWERS (designated by RLM)

Accountable Technical Individual. …………………………. J. Chrzanowski

Test Director

Independent Reviewer

D-Site Shift Supervisor

Independent

NCSX ………………….Steve Raftopoulos, Tom Meighan

Vacuum

Project Engineer for Stellerator Systems (WBS 1) Manager…….. Brad Nelson (ORNL)

WBS Manager for Modular Coils (WBS14).. ……………………Dave Williamson (ORNL)

Quality Assurance/Quality Control. ……………………………….Judy Malsbury

Maintenance and Operations Division

Energy Conversion System/Motor Control Division

Engineering ……………………………………..

Environmental Restoration & Waste Management Division

Environmental, Safety & Health……………………………………Jerry Levine

Industrial Hygiene………………………………………………... Bill Slavin

Health Physics…………………

RLM ………………………………………………………………..Larry Dudek

| TRAINING (designated by RLM) |
| --- |
| No training required ______________ | Instructor Jim Chrzanowski |
| Personnel (group, job title or individual name) | Read Only | Instruction Pre-job Briefing | Hands On |
| Lead Tech. |  | X |  |
| Technicians performing task |  | X |  |
| Field Supervisors |  | X |  |
| Quality Control Representative |  | X |  |
| Training Rep. |
| RLM Larry Dudek |

RECORD OF CHANGE

| Revision | Date | Description of Change |
| --- | --- | --- |
| 00 |  | Initial release |

TABLE OF CONTENTS

1	Scope	1

1.1	Introduction	1

1.2	Scope	1

1.3	Identification of winding form being prepared:	1

2	Applicable Documents	1

2.1	NCSX-MIT/QA-142-01:	1

2.2	NCSX-PLAN-MCWFOP-00:	1

3	Safety Requirements:	1

3.1	Job Hazard Analysis:	2

4	Prerequisites and Conditions	2

4.1	Pre-Job Briefing:	2

4.2	Daily Operations Startup and Shutdown:	2

4.3	Torque Values:	2

5	Materials and Parts for his Station	2

6	Fabrication Process	3

6.1	Daily Startup Activities:	3

6.2	Daily Shutdown Activities:	3

6.3	Transport of Winding Form to the Modular Coil Mfg. Facility (MCMF):	3

6.4	Verification of the Electrical Properties of the Poloidal Break [Not required for TRC]	3

6.5	Mount WF to Support Ring Assembly:	6

6.6	Install MCWF in Turning Fixture:	7

6.7	Visual Inspection	8

6.8	Cleaning Tapped Holes	9

6.9	Dimensional Inspection	9

6.10	Installation of Clamp Studs	9

6.11	Cleaning:	11

6.12	Mold Release:	11

6.13	Winding clamps	12

6.14	Inner wall copper cladding	12

6.15	Dimensional Inspection	13

6.16	Lead Terminal Block	14

6.17	Verification of the dielectric insulation at lead block	14

7	Station No. 1 Completion:	16

7.1	Document Verification:	16

7.2	Field Package:	16

7.3	Approval:	16

#### LIST OF FIGURES

Figure 1- Typical Poloidal Break	5

Figure 2-Mounting support brackets to casting	6

Figure 3-Position Casting in Assy. Fixture	6

Figure 4- Install Support Ring	7

Figure 5-Install Lifting Beam	7

Figure 6-Rotate Casting/Ring Assembly	7

Figure 7- Turning Fixture	8

Figure 8- Stud Weld Fixture	10

Figure 9- Mold Release and Masked Surfaces	11

Figure 10- Winding Clamps	12

Figure 11- Inner Copper Cladding	13

Figure 12- Lead Block	14

# Scope

## Introduction

The Modular Coil Manufacturing Facility is divided into 6 workstations.  Each workstation has a specific set of tasks that will be performed as part of the overall fabrication process.  The fabrication procedures will address the manufacturing, inspection, test and QC inspection points for a specific workstation.

- Station No. 1…	Winding Form Preparation & Post VPI Activities

- Station No. 2…	Winding Station A/ Molding and VPI Preparation

- Station No. 3…	Winding Station B/ Molding and VPI Preparation

- Station No. 4…	Winding Station C/ Molding and VPI Preparation

- Station No. 5…	VPI and Autoclave Activities

- Station No. 6…	Coil Testing Facility

## Scope

This procedure prepares each Modular Coil Winding Form (MCWF) or Twisted Racetrack Coil winding form (TRC) for winding.  It includes:

- Mounting the winding form to the turning fixture

- Verification of electrical integrity of poloidal break

- Winding Form inspection and measurements

- Installation of clamp studs

- Cleaning of winding form

- Installation of winding clamps

- Installation of the inner cladding plates

## Identification of winding form being prepared:

Station Number: ________ (Location where work will be performed)

Winding Form Type:  _______________ [Type A, B, C or Twisted Racetrack Coil (TRC)]

MC Winding Form ID No: _________________

Modular Coil Identification Number:  ___________

# Applicable Documents

## NCSX-MIT/QA-142-01:

All applicable documents associated with this procedure, are identified in the MIT/QA Plan, document number NCSX-MIT/QA-142-01.

## NCSX-PLAN-MCWFOP-00:

All Modular Coil work processes are governed by the “Winding Facility Operations Plan”, document number NCSX-PLAN-MCWFOP-00.

# Safety Requirements:

All work will be performed in a safe manner in accordance with PPPL safety policies ES&H 5008 and “Integrated Safety Management” (ISM) policy.

## Job Hazard Analysis:

A JHA will be generated for each workstation, identifying existing or potential workplace hazards and to evaluate the risk of worker injury or illness associated with job tasks. (Reference document ESH-004 “Job Hazard Analysis”)  The IH representative will review the JHA’s for accuracy as well as completeness.  It will be reviewed with all activity participants at the Pre-Job briefings.

# Prerequisites and Conditions

## Pre-Job Briefing:

A pre-job briefing will be held, describing the processes and safety issues prior to starting any part of this procedure.	  Attendance shall be documented via training sign-in sheet.

Pre job Briefing complete: ________________________________  _________________

MC Field Supervisor                           Date

## Daily Operations Startup and Shutdown:

Each working day, it is required to complete and initial the daily operations startup log to ensure that the station is ready to commence work activities for the day.  The signoff log is located in the back of this procedure.  See section 6.1 and 6.2 for details.

## Torque Values:

The following torque values shall be used for securing hardware unless otherwise specified in the procedure. (Low carbon steel hardware)

3/8-16UNC ……	18 ft-lbs		3/8-24UNF ……	19 ft-lbs

½-13 UNC ……	38 ft-lbs		½ -20 UNF ……	40 ft-lbs

5/8-11 UNC….	83 ft-lbs		5/8-18 UNF.…..	95 ft-lbs

¾-10 UNC..……	105 ft-lbs	¾-16 UNF …….	102 ft-lbs

1-8 UNC ………	236 ft-lbs	1-14 UNF ……..	212 ft-lbs

# Materials and Parts for his Station

The following materials and/or equipment will be used with this procedure.

| General Description | Material | Reference Document/Product No. |
| --- | --- | --- |
| Cladding | Copper | Drawing list to be added as addendum for each coil type as approved |
| Solvent | Chlorine-Free Degreaser | CRC Product No. 03185 [MSDS #05032] |
| Solvent | Acetone | MSDS# 00561 |
| Studs for coil clamp to casting stud | Stainless steel grade 316 | Drawing SE1405-265P |
| Mold release | Release agent dry lubricant | “Miller-Stephenson” -PTFE MS122DF |
| MC Turning Fixture | Equipment |  |
| Casting to Ring Assy. Fixture | Fixture |  |
| Weld stud alignment fixture | Fixture |  |
| Stud Welder unit | Equipment |  |
| Supports and hardware for mounting casting to turning rings | Fixture |  |
| Cladding insulation | Kapton-Type HN | 0.00325 inch thick |
| Double faced adhesive tape | 5 mil thick | Product no.9485PC-2 |
| Winding clamps | Equipment | Drawing SE144-080 |
| Alcohol | Ethanol | MSDS |

# Fabrication Process

This fabrication procedure is to be used as guide to complete the station no. 1 activities.  Deviation from this procedure can be made during the winding process with the concurrence of the MC Field Supervisor.  All deviations shall be documented in the procedure and initialed by the MC Field Supervisor.  Procedure changes need to be incorporated into document via “Minor Procedure Changes” or “Revisions”.

## Daily Startup Activities:

### Check all daily supplies needed:

### Turn on the Turning Fixture power switch to verify operation.

### Check stud welder for operation [Only if being used that day]

### Check station for cleanliness

### Check that the day’s travelers and procedures are in their document holder.

### Date and initial daily log at the back of procedure

## Daily Shutdown Activities:

### Turn off power to Turning Fixture.

### Turn off stud welder and secure for off hours.

### Clean entire workstation area.

### Verify that all Traveler and data sheet information is complete.

### The Lead Technician shall verify that the Station’s Log Book has been completed and signed for the day.

### Cover the Modular coil casting with plastic tarp.

### Date and initial daily log at the back of procedure

## Transport of Winding Form to the Modular Coil Mfg. Facility (MCMF):

### Transport a MCWF or TRC from its storage area to the MCMF.

#### Position the winding form on the floor supported by wooden blocks.

## Verification of the Electrical Properties of the Poloidal Break [Not required for TRC]

The electrical integrity of the poloidal break needs to be verified prior to mounting the MCWF into the support ring.  [See Figure 1- Typical Poloidal Break]

### Test Criteria

-  Test Voltage: 100 volts

-  Acceptance criteria for this test:  >500 k-ohms

- The Test Director for this test is: _____________________________

### Safety Requirements & Conditions

#### The following safety and prerequisites shall be used for performing test of the Poloidal break.

#### Technicians and engineers performing these tests shall be familiar with the hazards and work procedure to minimize accidents that may occur.

#### There shall be present a second person, “safety watch” monitoring the operator, and capable of removing the power in case of an accident.  This person shall be CPR qualified.

Qualified CPR Member: ______________________   Recert. Date: ____________

#### During the test, the “Test Area” shall be roped-off and suitable “danger high voltage” signs and flashing lights displayed.

Test Director Verify: ___________________________

#### The test operator shall stand on an electrical safety mat during the test operation.

#### Approved rubber electrical safety gloves shall be worn by test members during grounding operations which occur once the test has been completed, and the test equipment turned off.

#### Upon completion of test and before the components are declared safe to touch, (dielectric joint) being tested shall be properly discharged using a “Ground Hook”.  After a minimum period of 10 seconds, while the ground hook is still in place, attach a ground cable to the casting and poloidal mid-plane.  The ground hook may be removed once the ground cable is in place.

### Testing of Mid-Plane Insulation:

#### Electrically connect (jumper) the poloidal joint mid-plane to the modular coil for this test.

#### Measure the insulation resistance between the mid-plane plate and each bolt. The test results shall be in compliance with the requirements noted in Section 6.4.1.

Mid-Plane to Each Bolt- Megger Test Results

| Test Components | Voltage Level Volts | Resistance k-Ohms | Remarks |
| --- | --- | --- | --- |
| Bolt 1 to Mid | 100 |  |  |
| Bolt 2 to Mid | 100 |  |  |
| Bolt 3 to Mid | 100 |  |  |
| Bolt 4 to Mid | 100 |  |  |
| Bolt 5 to Mid | 100 |  |  |
| Bolt 6 to Mid | 100 |  |  |
| Bolt 7 to Mid | 100 |  |  |

Equipment ID Number:__________________________	Calibration Date: _____________

Megger Results: Acceptable: _______________ Unacceptable: ____________

Test Director Signoff: _____________________________ Date: ______________

Quality Control Witness: __________________________ Date: ______________

Remarks:

### Testing of Bolt Insulation

#### Electrically connect (jumper) together all of the bolts and the modular coil winding form for this test.

#### Measure the insulation resistance between the electrically connected (jumpered) combination and the mid-plane.  The test results shall be in compliance with the requirements noted in Section 6.1.4

Mid-Plane to Bolts & Winding Form- Megger Test Results

| Test Components | Voltage Level Volts | Resistance k-Ohms | Remarks |
| --- | --- | --- | --- |
| Mid-plane to Bolts & WF | 100 |  |  |

Equipment ID Number:__________________________	Calibration Date: _____________

Megger Results: Acceptable: _______________ Unacceptable: ____________

Test Director Signoff: _____________________________ Date: ______________

Remarks:

Figure 1- Typical Poloidal Break

### If the test results were within the test criteria identified in section 6.4.1 proceed to section 6.5.

### If the test results were unacceptable, under the direction of the field supervisor, take corrective action to make repairs, and repeat the electrical tests.

## Mount WF to Support Ring Assembly:

### Mount the appropriate support brackets to the casting that will allow the winding form to be joined with the Turning Fixture support ring. (Figure 2-Mounting support brackets to casting)

### Note: Each coil type (A, B, C, TRC) have different support brackets that will join the MCWF to Turning Fixture support rings.

### Position the winding form with support brackets into the assembly fixture. (Figure 3-Position Casting in Assy. Fixture) [Note: the TRC will not be assembled in the assembly fixture]

### Install a support ring into the assembly fixture around the casting, and secure winding form and support ring together. (Figure 4- Install Support Ring)

### Secure the support/lifting beam to the MCWF /Ring Assembly (MCCRA). (Figure 5-Install Lifting Beam)

### Verify that all hardware has been torqued and that casting is ready for transport to Turning Fixture.

Verified:

Lead Technician: ____________________________ Date: ____________________

Field Supervisor: ____________________________ Date: ____________________

### To ensure proper alignment and operation of the turning fixture, rotate the MCWF a full revolution using the foot-pedal control.  Re-adjust the alignment rollers as required.   Alignment of MCWF to the turning fixture is complete.

Verified by: _________________________ Date: __________________

Lead Technician

Figure 2-Mounting support brackets to casting

Figure 3-Position Casting in Assy. Fixture

Figure 4- Install Support Ring

Figure 5-Install Lifting Beam

Figure 6-Rotate Casting/Ring Assembly

## Install MCWF in Turning Fixture:

### Carefully raise the MCCRA until it is in the vertical position.  (Figure 6-Rotate Casting/Ring Assembly) Transport and install MCCRA into the Station No. 1 turning fixture using lift procedure D-L-NCSX-983.  Secure the MCWF and ring assembly to the turning fixture.

Verified by: _________________________ Date: __________________

Field Supervisor

### Align the guide rollers to the support ring.

### Verify that the support ring gear rack is engaged with the drive unit.

Verified by: _________________________ Date: __________________

Lead Technician

### Verify that the upper support/lift beam is in proper position and secured with appropriate hardware that that is torqued to the proper value.

Verified by: _________________________ Date: __________________

Lead Technician

### Remove the upper support plates between the support ring and lift beam.  This operation must be verified prior to operating turning fixture.

Verified by: _________________________ Date: __________________

Lead Technician

Figure 7- Turning Fixture

## Visual Inspection

Perform a visual inspection of the casting. Look for any obvious defects or damage as a result of shipment.  Check each threaded hole with bolt.  Re- tap as required RECORD FINDINGS

Inspection Findings:

Inspection Performed by: _________________________ Date: __________________

## Cleaning Tapped Holes

Using a bottlebrush, clean cotton rags and “Chlor-Free Degreaser”; thoroughly clean the tapped holes in the MCWF removing any chips or oil residue remaining from the casting manufacturing process.

Verified by: _________________________ Date: __________________

Lead Technician

## Dimensional Inspection

### Using metrology equipment (Romer arm and scanner) thoroughly measure the MCWF winding surfaces. Include all results in the MC traveler package.  These measurements should be compared to models provided by NCSX engineering.  All deviations shall be documented and any deviations dispositioned by the NCSX project prior to proceeding.

### Procedure D-NCSX-MCF-005 describes the use of the “Romer” measuring arm that will be used. All data will be attached to the back of the procedure

Measurements completed by:  _________________________ Date: _______________

Summary of Results:

Measurements completed and verified by:

Field Supervisor: ____________________________ Date: ____________________

QC Representative: ____________________________ Date: ____________________

## Seal Poloidal Break

### Seal the poloidal break seam using RTV 108 sealant. Apply over all seams that will be inside of the Bag mold. Smooth RTV with putty knife.  This seal is required for successful VPI operations.

Verified by: _________________________ Date: __________________

Lead Technician

## Installation of Clamp Studs

Install stainless steel studs on each side of the castings for the winding and coil clamps.  All welding shall be performed by weld certified individuals.

### Notify the ESU and obtain a flame permit prior to starting welding operation.

#### Lead Technician verify: _____________________ Date: ________________

### Position the stud alignment fixture onto the casting using the inner web tapped hole to secure the fixture in place.

Figure 8- Stud Weld Fixture

### Using the stud welder, weld grade 316 stainless steel studs (reference drawing SE1405-265P) on each side of the winding.  Studs shall be positioned per appropriate coil drawings. In some inaccessible locations it may be necessary to TIG weld the studs in position.

Stud Welder Settings:

### After welding, remove the alignment fixture and clean the weld.  Remove all excess weld material.

### Repeat process for each clamp position, until all studs have been installed.

### Each welded stud shall be inspected by a QC weld inspector (100% inspection).   Welded studs rejected by QC will be removed, surface cleaned and replaced with a new stud.  Attach all QC inspection reports to procedure.

#### Stud Weld performed by: _____________________ Date: ________________

#### Q.C. Inspection: _____________________ Date: ________________

Summary of Results:

## Cleaning:

Using CRC Industrial “Chlor-Free Degreaser and clean cotton cloths thoroughly clean (wipe down) the entire MCWF.  Then wipe surface using Ethanol and clean cloths.

#### Lead Technician verify: _____________________ Date: ________________

## Mold Release:

Mask the surfaces identified in Figure 9.  Apply (3) coats of mold release (“Miller-Stephenson”-PTFE MS122DF) to the winding surfaces.  Allow each coat to dry to the touch prior to applying the next coat.   Figure 9- Mold Release and Masked Surfaces identifies the surfaces to be coated and masked.

Figure 9- Mold Release and Masked Surfaces

#### Lead Technician verify: _____________________ Date: ________________

## Winding clamps

Mount the (3) part winding clamps to the MCWF as shown in Figure 10- Winding Clamps.  The clamps are located approximately every 3 inches along the entire length of the MCWF.  Secure the winding base to the top of the tee using the appropriate hardware.  Position the (2) side bars to the winding base, and side studs using the appropriate hardware.

Figure 10- Winding Clamps

## Inner wall copper cladding

### Select the inner wall copper cladding being used for the coil type being manufactured.  Clean the copper plates with CRC Industrial “Chlor-Free Degreaser and clean cotton cloths.  EXTREME CARE must be taken during handling of the cladding because of the sharp edges.

### Fitup each section of copper cladding to the inner wall using the cladding mapping drawings.  Customizing of each section of copper cladding will be required. (Figure 11- Inner Copper Cladding)

### Once all of the cladding have been fit, remove and re-clean the plates.  Check that there are no sharp edges or burrs.

### Apply (2) layers of adhesive backed Kapton tape (0.00325 in. thick) to the side of the cladding facing the winding surfaces.

### Secure the insulated cladding to the winding form winding surfaces using double face 3M adhesive tape.

### During the installation of the cladding, continue to verify that the cladding is electrically isolated from the winding form using a multi-meter.

Equipment Name & ID Number:______________________	Calibration Date: ___________

Figure 11- Inner Copper Cladding

Installation of the Inner Copper Cladding is complete and dielectric break is verified:

Lead Technician: ____________________________ Date: ____________________

Field Supervisor: ____________________________ Date: ____________________

Quality Control: _____________________________ Date: ____________________

## Dimensional Inspection

### Once the copper cladding has been installed, remeasure the winding surface using metrology equipment (Romer arm and scanner). Include all results in the MC traveler package.  These measurements should be compared to models provided by NCSX engineering.

### Procedure D-NCSX-MCF-005 describes the use of the “Romer” measuring arm that will be used. All data will be attached to the back of the procedure

Measurements completed by:  _________________________ Date: _______________

Summary of Results:

Measurements completed and verified by:

Field Supervisor: ____________________________ Date: ____________________

QC Representative: ____________________________ Date: ____________________

## Lead Terminal Block

### Assemble the lead terminal block components to the outside of the casting per the coil drawings.

Terminal Block Installed:

Lead Technician: ____________________________ Date: ____________________

Figure 12- Lead Block

## Verification of the dielectric insulation at lead block

The electrical integrity of the terminal block needs to be verified prior to starting the coil winding.

### Test Criteria

-  Test Voltage: ______________________ volts

-  Acceptance criteria for this test:  > _______________________ k-ohms

- The Test Director for this test is: _____________________________

### Safety Requirements & Conditions

#### The following safety and prerequisites shall be used for performing test of the Poloidal break.

#### Technicians and engineers performing these tests shall be familiar with the hazards and work procedure to minimize accidents that may occur.

#### There shall be present a second person, “safety watch” monitoring the operator, and capable of removing the power in case of an accident.  This person shall be CPR qualified.

Qualified CPR Member: ______________________   Recert. Date: ____________

#### During the test, the “Test Area” shall be roped-off and suitable “danger high voltage” signs and flashing lights displayed.

Test Director Verify: ___________________________

#### The test operator shall stand on an electrical safety mat during the test operation.

#### Approved rubber electrical safety gloves shall be worn by test members during grounding operations which occur once the test has been completed, and the test equipment turned off.

#### Upon completion of test and before the components are declared safe to touch, the dielectric joint being tested shall be properly discharged using a “Ground Hook”.  After a minimum period of 10 seconds, while the ground hook is still in place, attach a ground cable to the casting and poloidal mid-plane.  The ground hook may be removed once the ground cable is in place.

### Testing of Mid-Plane Insulation:

#### Electrically connect (jumper) the inner connectors together together this test.

#### Ground (3) of the layers together, and apply the specified voltage to the 4th. Measure the insulation resistance between each layer (terminal set) of connectors. The test results shall be in compliance with the requirements noted in Section 6.17.1.

Megger Test Results

| Voltage Level Volts | Resistance k-Ohms | Remarks |
| --- | --- | --- |
| Layer 1 |  |  |
| Layer 2 |  |  |
| Layer 3 |  |  |
| Layer 4 |  |  |

Equipment ID Number:__________________________	Calibration Date: _____________

Megger Results: Acceptable: _______________ Unacceptable: ____________

Test Director Signoff: _____________________________ Date: ______________

Quality Control Witness: __________________________ Date: ______________

Remarks:

# Station No. 1 Completion:

## Document Verification:

Verify that all pertinent data on the procedure and data sheets have been completed.

## Field Package:

Ensure that all data sheets, photographs, QC inspection sheets, etc are included in the Field Package.

## Approval:

Prior to releasing a modular coil from one station to the next it is required that the all-responsible individuals sign the release indicating that all processes at that station have been satisfactorily completed.  The release will include signatures from the Station Lead Technician, Field Supervisor and the QC representative.

All winding form preparation activities have been satisfactorily completed and the winding form is ready for transfer to the next station:

Lead Technician: ____________________________ Date: ____________________

Field Supervisor: ____________________________ Date: ____________________

Quality Control: _____________________________ Date: ____________________

Comments:

Daily Start-Up Log- Station 1

| Date | Lead Tech Initial | Date | Lead Tech Initial | Date | Lead Tech Initial |
| --- | --- | --- | --- | --- | --- |

Daily Shutdown Log- Station 1

| Date | Lead Tech Initial | Date | Lead Tech Initial | Date | Lead Tech Initial |
| --- | --- | --- | --- | --- | --- |

# Text boxes

Sidebars

Mid-plane connection

Winding Base

Masked areas

Turning Fixture Support Frame

Turning Fixture Support Ring Guide Rollers

Turning Fixture Drive System

Turning Fixture-Upper Support/Lifting Beam

Turning Fixture Support Plates & spaces assembly

Areas identified with “V” marks are to be mold released.

Turning Fixture Support Ring