# NCSX

# Specification

# TF Coil Conductor Specification

# NCSX-CSPEC-131-02-00

# Draft B

# 5 May 2005

Prepared by: __________________________________________________________________________

M. Kalish, NCSX WBS 13 Manager

Concur: ______________________________________________________________________________

J. Chrzanowski, Technical Expert

Concur: ______________________________________________________________________________

B. Nelson, Project Engineer for Stellarator Core Systems (WBS 1)

Concur: ______________________________________________________________________________

Frank Malinowski, NCSX Quality Assurance Representative

Approved by: _________________________________________________________________________

W. Reiersen, Engineering Manager

Controlled Document

THIS IS AN UNCONTROLLED DOCUMENT ONCE PRINTED

Check the NCSX Engineering Web prior to use to assure that this document is current.

# Record of Revisions

| Revision | Date | Description of Changes |
| --- | --- | --- |
| Rev. 0 |  | Initial issue |

# TABLE OF CONTENTS

1	Scope	1

2	Applicable Documents	1

3	Requirements	1

3.1	Item Definition	1

3.2	Design and Construction	1

3.2.1	Conductor Geometry	1

3.2.1.1	Conductor Height and Width	1

3.2.1.2	Conductor Hole	1

3.2.1.3	Conductor Length	1

3.2.2	Conductor Characteristics	1

3.2.2.1	Copper Grade	1

3.2.2.2	Hardness	2

3.2.2.3	Strength	2

3.2.2.4	Conductor Resistance	2

3.2.2.5	Conductor Weight	2

3.2.2.6	Conductor Integrity	2

3.2.3	Standards of Manufacture	2

3.2.3.1	Lubricants	2

3.2.3.2	Cleanliness	2

4	Quality Assurance Provisions	2

4.1	General	2

4.1.1	Responsibility for Inspection	2

4.2	Quality Conformance Inspections	2

4.2.1	Verification of Conductor Resistance	2

4.2.2	Verification of Conductor Dimensions	3

4.2.2.1	Conductor Width and Height	3

4.2.2.2	Conductor Hole	3

4.2.2.3	Conductor Length	3

4.2.3	Verification of Copper Grade	3

4.2.4	Verification of Conductor Weight	3

4.2.5	General Inspection	3

4.2.6	Verification of Material Properties / Testing	3

4.2.6.1	Test Specimens	3

4.2.6.2	Yield Testing	3

4.2.6.3	Tensile Testing	3

4.2.6.4	Hardness Testing	3

4.2.6.5	Resistivity Testing	4

4.2.7	Verification of Preparation for Shipping	4

5	Preparation for Delivery	4

5.1	Conductor Spooling	4

5.2	Conductor Protection	4

5.3	Crating	4

5.4	Shipping	4

6	Attachment	5

# TABLE OF FIGURES

Figure 1 - Conductor and spool layout	4

# Scope

The National Compact Stellarator Experiment (NCSX) is an experimental research facility that is to be constructed at the Department of Energy’s Princeton Plasma Physics Laboratory (PPPL). Its mission is to acquire the physics knowledge needed to evaluate compact stellarators as a fusion concept, and to advance the understanding of three-dimensional plasma physics for fusion and basic science.

The TF Coils are a Primary component of the NCSX Device.  Eighteen equally spaced D shaped coils surround the core of the machine.  Each of these 12 turn coils is wound using a solid copper conductor with an extruded center hole for liquid nitrogen cooling.  This specification establishes the manufacturing and acceptance requirements for the copper conductor that will be used in the fabrication of the TF Coils.  It defines the alloy, form, quantity and integrity of the hollow extruded copper conductor. To minimize the risk of coil failure, strict adherence to these specifications is essential.

# Applicable Documents

TF Coil Conductor Detail SE131-014

# Requirements

## Item Definition

The item is a continuous length of extruded copper conductor with a center hole wound into a pancake spool.

## Design and Construction

### Conductor Geometry

#### Conductor Height and Width

The conductor height and width shall conform to the conductor outline drawing SE131-014

#### Conductor Hole

The conductor shall be extruded with a continuous .312 inch +/-0.005 inch diameter hole centered on the conductor cross section within +/-0.010 inch

#### Conductor Length

Each individual spool shall be wound in a continuous length with no splices.  The conductor shall be a minimum of 100 ft long and a maximum of 110 ft long.

### Conductor Characteristics

#### Copper Grade

The material required is CDA No. 10700 oxygen-free copper with silver content of 25 troy oz/ton (.085% Ag).  .  The material shall be of such quality and purity that the finished product shall have the properties and characteristics prescribed in this specification and shall be cold drawn to produce the required temper.  The conductors shall be furnished in the cold drawn condition.

#### Hardness

The conductor shall have a Rockwell Hardness F between 60 and 70.  If there is a discrepancy between the Hardness requirement and the Yield Strength requirement the Yield Strength measurement shall be the governing requirement.

#### Strength

Yield Strength shall be 26,000 psi min. to 30,000 psi max. (0.5% elongation)

Ultimate Tensile Strength shall be 36,000 psi minimum @ 15% elongation

#### Conductor Resistance

Electrical conductivity shall be 100% minimum IACS.  Table I, ASTM A188, for resistivity of cold drawn copper.

#### Conductor Weight

The weight of the raw conductor shall be 235.3 +/- 4 pounds per 100 feet.

#### Conductor Integrity

The hole profile shall show neither re-entrant material or notches greater than 0.020 inch. Cracks, laps, fold, scale and any other discontinuity longer than 0.020 inch normal to the hole surface, shall not be visible when inspected at 100x magnification.

### Standards of Manufacture

#### Lubricants

The Subcontractor shall ensure that the finished conductor has been thoroughly cleaned with a solvent adequate for the removal of any trace amounts of lubricants that may have been used.

#### Cleanliness

The Subcontractor shall take the necessary precautions to ensure that the finished conductor is clean, free of any oils, or dirt related to processing or handling.

# Quality Assurance Provisions

## General

### Responsibility for Inspection

The responsibility for performing all tests and verifications rests with the supplier. PPPL reserves the right to witness or separately perform all tests specified or otherwise inspect any or all tests and inspections.  Methods used for inspection shall be proposed by Subcontractor and approved by PPPL

## Quality Conformance Inspections

This section provides the conformance and testing requirements for the requirements specified in Sections 3 and 5.

### Verification of Conductor Resistance

A resistance measurement shall be made to verify compliance with Section 3.2.2.4

### Verification of Conductor Dimensions

#### Conductor Width and Height

The conductor width and height shall be measured to verify compliance with Sections 3.2.1.1.  Six measurements shall be taken at the start of the conductor length, in the middle of the conductor length, and at the end of the conductor length.  The six measurements at these locations shall be six inches apart.  Measurements at the start and end of the conductor shall be at least 12 inches from terminus of the conductor.

#### Conductor Hole

Conductors shall be checked to verify that the centering of the cooling hole is within the required tolerance.

#### Conductor Length

The Subcontractor shall provide an in-process measurement of the conductor length to verify compliance with Section 3.2.1.3.

### Verification of Copper Grade

Material certifications shall be provided to verify compliance with Section 3.2.2.1.

### Verification of Conductor Weight

The weight of the cable shall be measured to verify compliance with Section 3.2.2.5.

### General Inspection

The finished material shall be free from blisters, slivers, laps, seams, cracks and scale, as well as from all other imperfections, such as damaged corners or edges, not consistent with best commercial practice.

### Verification of Material Properties / Testing

#### Test Specimens

A minimum of 10% of the spools shall be selected to provide samples for testing i.e. for 77 spools eight sets of test samples are required.  In addition there must be at least two sets of samples from a group of spools that came from a unique lot of billets.  If there are fewer than twenty spools that were manufactured from a particular lot of material there must still be a minimum of two sets of test samples from that group of spools.  A “set of test samples” refers to the a group of test pieces required to provide the yield, tensile, and hardness testing.

#### Yield Testing

Specimens are to be tested to verify yield strength per section 3.2.2.3

#### Tensile Testing

Specimens are to be tested to verify tensile strength per section 3.2.2.3

#### Hardness Testing

The conductor shall be tested along its length every 10 ft to verify the hardness specified in section 3.2.2.2.   The test specimens used to test for yield and tensile strength shall be tested for hardness prior to being pulled so that a correlation between hardness and yield can be documented.

#### Resistivity Testing

Specimens shall be subjected to the electrical resistivity test as prescribed in ASTM B193

### Verification of Preparation for Shipping

The Subcontractor shall verify compliance with the requirements for conductor spooling (Section 5.1), conductor protection (Section 5.2), and crating (Section 5.3)

# Preparation for Delivery

## Conductor Spooling

The conductor will be wound with the wide side (0.966 inch) of the conductor lying flat.  The spool will be wound against the narrow .709 dimension bending the coil the “hard way” into a single pancake layer.  The inner diameter of the spool will be of a diameter between 36” and 38”.  There will be only one continuous length of conductor per spool.  The spools shall be independently restrained with non metallic bands or by other means so that when removed from the crate they can be handled without unwinding.

36” to 38”

.966”

.709”

Figure 1 - Conductor and spool layout (not to scale,  figure only imparts orientation of conductor)

## Conductor Protection

Each spool of conductor will be plastic wrapped to protect the conductor from dirt and foreign materials.

## Crating

The spools shall be crated to protect the conductor from shock and weather conditions, including precipitation. The crate shall be built for handling with slings from overhead cranes, and transport by forklifts.  Container to be approved by PPPL before shipping.

## Shipping

- Subcontractor is responsible arranging shipment, and for the safe arrival of the item at PPPL in Princeton, New Jersey, USA.  Subcontractor’s name, shipper, purchase order number, contents and gross weight shall be marked on the shipping container.

- Subcontractor shall have a signed "Product Quality Certification and Shipping Release" Form (see Section 6) prior to PPPL acceptance of procured items or services for full or partial shipment. PPPL reserves the right to refuse to accept shipments unless accompanied by a signed " Product Quality Certification and Shipping Release" Form.

# Attachment

Attached is the “Product Quality Certification and Shipping Release" Form.