NCSX

Product Specification

For The

Modular Coil Assembly

NCSX-CSPEC-142-05-00

DRAFT E

29 October 2005

Prepared by: __________________________________________________________________________

D. Williamson, Modular Coil System (WBS 14) Manager

Concur: ______________________________________________________________________________

J. Chrzanowski, ATI for Modular Coil Fabrication

Concur: ______________________________________________________________________________

L. Dudek, RLM for Modular Coil Fabrication

Concur: ______________________________________________________________________________

B. Nelson, RLM for Stellarator Core Systems (WBS 1) Design and Procurement

Concur: ______________________________________________________________________________

F. Malinowski, Quality Assurance

Approved by: _________________________________________________________________________

W. Reiersen, Engineering Manager

Record of Revisions

| Revision | Date | ECP | Description of Change |
| --- | --- | --- | --- |
| Rev. 0 | 10/30/05 | --- | Initial Release |

Table of Contents

1	Scope	1

2	Applicable Documents	1

2.1	NCSX Documents	1

2.2	Other Documents	1

3	Requirements	1

3.1	Item Definition	1

3.2	Characteristics	3

3.2.1	Performance	3

3.2.1.1	Design Verification	3

3.2.1.2	Timeline for Coil Cool-down to Cryogenic Temperature	3

3.2.1.3	Coil Warm-up Timeline	3

3.2.1.4	Cool-down and Warm-up Cycles	3

3.2.1.5	Coil Temperatures during Bakeout	3

3.2.1.6	Bakeout Cycles	4

3.2.1.7	Pre-Pulse Temperature	4

3.2.1.8	Field Error Requirements	4

3.2.1.8.1	Poloidal Electrical Breaks	4

3.2.1.8.2	Winding Tolerance	4

3.2.1.9	Reference Scenario Requirements	4

3.2.1.10	Pulse Repetition Rate	5

3.2.1.11	Electrical Requirements	5

3.2.1.11.1	Electrical Isolation of the Conductor	5

3.2.1.11.2	Turn-to-turn Voltage Standoff	5

3.2.1.11.3	Electrical Isolation and Grounding of Other Components	5

3.2.1.11.4	Electrical Resistance	6

3.2.2	Physical Characteristics	6

3.2.2.1	Winding Form	6

3.2.2.2	Attachments	7

3.2.2.3	Winding Packs	7

3.2.2.3.1	Cladding	7

3.2.2.3.2	Chill Plates and Coolant Tubes	7

3.2.2.3.3	Conductor	7

3.2.2.3.4	Ground Insulation	7

3.2.2.3.5	Lead Blocks	7

3.2.2.3.6	Lead Assembly	7

3.2.2.3.7	Clamps	8

3.2.2.3.8	Co-wound Diagnostic Loops	8

3.2.2.3.9	Instrumentation	8

3.2.2.3.10	Bag Mold Assembly	8

3.2.2.4	Weight	8

3.2.3	System Quality Factors	8

3.2.3.1	Reliability, Availability, and Maintainability	8

3.2.3.2	Design Life	9

3.2.4	Transportability	9

3.2.5	Interface Requirements	9

3.2.5.1	Vacuum Vessel System (WBS 12) Interface Requirements	9

3.2.5.2	Conventional Coils (WBS 13) Interface Requirements	10

3.2.5.3	Coil Support Structures (WBS 15) Interface Requirements	10

3.2.5.4	Liquid Nitrogen Distribution System (WBS 161)	10

3.2.5.5	Electrical Power Systems (WBS 4)	10

3.2.5.6	Central I&C (WBS 5)	11

3.3	Design and Construction	11

3.3.1	Materials, Processes, and Parts	11

3.3.1.1	Production Drawings	11

3.3.1.2	Magnetic Permeability	11

3.3.1.3	Corrosion Prevention and Control	11

3.3.1.4	Flammable Materials	11

3.3.1.5	Metrology	11

3.3.2	Labels	11

3.3.3	Workmanship	12

3.3.4	Interchangeability	12

4	Quality Assurance Provisions	12

4.1	General	12

4.2	Verification Methods	12

4.3	Quality Conformance	13

4.3.1	Verification of Design Verification Requirement	13

4.3.1.1	Verification of Coil Cool-down and Warm-up Timelines	13

4.3.1.2	Verification of Cool-down and Warm-up Cycles	13

4.3.1.3	Verification of Coil Temperatures during Bakeout	13

4.3.1.4	Verification of Bakeout Cycles	13

4.3.1.5	Verification of Pre-Pulse Temperature	13

4.3.1.6	Verification of Field Error Requirements	13

4.3.1.6.1	Verification of the Poloidal Electrical Breaks	13

4.3.1.6.2	Verification of Electrical Isolation	13

4.3.1.6.3	Verification of Winding Tolerance	13

4.3.1.7	Verification of Reference Scenario Requirements	14

4.3.1.8	Verification of Pulse Repetition Rate	14

4.3.1.9	Verification of Electrical Requirements	14

4.3.1.9.1	Verification of Electrical Isolation of the Conductor	14

4.3.1.9.2	Verification of Electrical Isolation and Grounding of Other Components	14

4.3.1.9.3	Verification of Electrical Resistance	14

4.3.2	Verification of Physical Characteristics	15

4.3.2.1	Winding Form	15

4.3.2.2	Attachments	15

4.3.2.3	Winding Packs	15

4.3.2.4	Cladding	15

4.3.2.5	Chill Plates and Tubes	15

4.3.2.6	Conductor	15

4.3.2.7	Ground Insulation	15

4.3.2.8	Lead Blocks	15

4.3.2.9	Terminal Assembly	15

4.3.2.10	Clamps	16

4.3.2.11	Diagnostic Loops	16

4.3.2.12	Instrumentation	16

4.3.2.13	Bag Mold Assembly	16

4.3.2.14	Weight	16

4.3.3	Verification of System Quality Factors	16

4.3.3.1	Reliability, Availability, and Maintainability	16

4.3.3.2	Design Life	16

4.3.3.3	Transportability	16

4.3.4	Verification of Interface Requirements	16

4.3.4.1	Vacuum Vessel	16

4.3.4.2	Conventional Coils	16

4.3.4.3	Coil Support Structures	17

4.3.4.4	Liquid Nitrogen Distribution System	17

4.3.4.5	Electrical Power Systems	17

4.3.4.6	Central I&C	17

5	Appendices	18

5.1	Assembly Models and Drawings	18

Table of Figures

Figure 3-1 Type-C Assembly	1

Figure 3-2 Terminal Assembly Isometric View	2

Figure 3-3 Electrical isolation and grounding of coolant loops	6

# Scope

The Modular Coil System (WBS 14) consists of eighteen (18) modular coils.  There are three (3) types of modular coils and six (6) of each type.  The three types of modular coils are Type-A, Type-B, and Type-C.  This specification defines the modular coil assembly (the Assembly) and requirements for its fabrication.

# Applicable Documents

## NCSX Documents

NCSX-ASPEC-GRD, NCSX General Requirements.  This document is referred to herein as the GRD.

NCSX-BSPEC-14-00, System Requirements for the Modular Coil System (SRD)

NCSX-CSPEC-14-01, Product Specification for the Three-Coil Assembly.

NCSX-CSPEC-141-03, Product Specification for the Modular Coil Winding Forms

NCSX-CSPEC-142-03, Product Specification for the Modular Coil Conductor

NCSX-CRIT-CRYO, Structural and Cryogenic Design Criteria

## Other Documents

ASTM A703/M-01, Specification for Steel Castings

ASTM B152/M-00, Standard Specification for Copper Sheet

ASTM B280-03, Standard Specification for Seamless Copper Tube

# Requirements

## Item Definition

The Assembly consists of a winding form with a machined tee profile onto which a coil is wound and is illustrated in Figure 3-1.  Major components of the Assembly are listed below.

Figure 3-1 Type-C Assembly

Winding Form. The Type-C winding form (the Winding Form) is a cast stainless steel structure with a machined “tee” feature.  The Product Specification for the Modular Coil Winding Forms (NCSX-CSPEC-141-03) defines the Winding Form and requirements for its fabrication.  The Winding Form will be fabricated in industry and delivered to PPPL as a completed assembly.

Winding Clamp Studs. After delivery to PPPL, studs will be welded to the base of the tee below the groove used to seal the bag mold.  The studs hold the side pieces of the winding clamps during coil fabrication.  Special clamp stud adapters will be required in some locations where the side of the base is not parallel to the tee.

Cladding. The cladding is a layer of copper that lies against the tee and cools the winding pack by conduction to the chill plates.

Chill Plates. The chill plates are the outer layer of copper and coolant tubes for LN2 cooling.  The chill plates are mechanically connected to the cladding.

Conductor. The conductor is stranded copper wire compacted into a rectangular cross-section and wrapped in fiberglass insulation.  The Product Specification for the Modular Coil Conductor (NCSX-CSPEC-142-03) defines the insulated conductor and requirements for its fabrication.  The Conductor will be fabricated in industry and delivered to PPPL on spools ready for coil manufacture.

Ground Insulation. The ground insulation consists of fiberglass and Kapton tape surrounding the winding pack.

Lead Blocks. The lead blocks are insulated supports for conductor entry and exit from winding pack.

Terminal Assembly. The Terminal Assembly consists of the hardware required to electrically connect the conductors from Side A winding pack to the Side B winding pack and to the electrical power feed.  This hardware includes the base blocks, insulators, jumpers, and lugs.  The Terminal Assembly is illustrated in Figure 3-2.

Figure 3-2 Terminal Assembly Isometric View

Clamps. There are two sets of clamps.  Winding clamps are used to position and hold the winding packs during coil fabrication.  Production clamps serve to provide lateral (toward the tee) and vertical (toward the base of the tee) preloads on winding pack.

Co-wound Diagnostic Loops. Two co-wound diagnostic loops are included in the Assembly.  They are terminated in a Pomona-C box mounted on the winding form.

Instrumentation. Assembly instrumentation includes strain gages, thermocouples, and voltage taps.

Bag Mold Assembly. The bag mold consists of strips of self-vulcanizing silicone rubber tape that is used to provide a vacuum barrier around the winding packs for vacuum pressure impregnation (VPI).  The bag mold is sealed to the Winding Form at the base of the tee with copper tubing inserted into a groove.  G-11CR pads are placed under the bag mold to provide a flat surface for the clamps to push against.  The bag mold is sealed by painting it with room temperature vulcanizing silicone (RTV).  After VPI, the glass/epoxy shell is removed and the bag mold is cut away from the G-11CR pads.  The winding clamps are removed and the production clamps are installed.  The G-11CR pads are the only elements of the bag mold assembly that provide a required function for coil operation.

## Characteristics

### Performance

#### Design Verification

The first article shall be instrumented such that key performance parameters (stresses, deflections, temperatures, pressures, etc.) can be measured and compared to calculated values to assure that the Assembly is performing consistent with expectations prior to First Plasma. [Ref. SRD Section 3.2.1.1.1.3 Design Verification]

#### Timeline for Coil Cool-down to Cryogenic Temperature

The Assembly shall be capable of being cooled down from room temperature (293K) to the pre-pulse operating temperature within 96 hours with the vacuum vessel at room temperature (20°C).  [Ref. SRD Section 3.2.1.2.2.1 Timeline for Coil Cool-down to Cryogenic Temperature]

#### Coil Warm-up Timeline

The modular coils shall be capable of being warmed up from operating temperature (80K) to room temperature (293K) within 96 hours.  [Ref. SRD Section 3.2.1.3.1 Coil Warm-up Timeline]

#### Cool-down and Warm-up Cycles

The design of the Assembly shall allow for at least 150 cool-down and warm-up cycles between room temperature and cryogenic temperature. [Ref. SRD Section 3.2.1.2.2.2 Cool-down and Warm-up Cycles]

#### Coil Temperatures during Bakeout

During bakeout of the vacuum vessel (up to 350ºC in the vacuum vessel shell and 150ºC at the ends of the port extensions), the temperature of the Assembly shall be capable of being kept below 90K and returned to their pre-pulse operating temperatures within the 24 hours following completion of bakeout.  [Ref. SRD Section 3.2.1.2.3.1 Coil Temperatures during Bakeout]

#### Bakeout Cycles

The Assembly shall be designed for at least 1000 bakeout cycles over the life of the machine.  [Ref. SRD Section 3.2.1.2.3.2 Bakeout Cycles]

#### Pre-Pulse Temperature

The modular coils shall return to a pre-pulse temperature of about 80K, so as to prevent overheating during repeated operation, with a vacuum vessel shell temperature in the range of 40ºC to 250 C.  [Ref. SRD Section 3.2.1.2.4]

#### Field Error Requirements

Background

Field errors are a major concern in the design of the modular coils.  The fundamental global requirement is that the toroidal flux in island regions due to fabrication errors, magnetic materials, and eddy currents shall not exceed 10% of the total toroidal flux in the plasma (including compensation).  To implement this requirement, external trim coils have been provided for field error correction.  Poloidal and toroidal electrical breaks are required in the modular coil structure to reduce the size of the eddy current loops and to reduce the longest eddy current time constant in the modular coils such that the calculated field errors are acceptably low.  The electrical breaks also facilitate field penetration from the modular and conventional (PF, TF and external trim) coils.  The modular coils will be fabricated and assembled to tight tolerances which are calculated to introduce acceptably low field errors (after correction).

##### Poloidal Electrical Breaks

- A poloidal electrical break shall be provided within each Assembly.  [Ref. SRD Section 3.2.1.2.5.1.2a Poloidal Electrical Breaks]

- The resistance of the insulation and of the bolt insulation shall be >500 k-ohms when tested at 100 VDC. [Ref. SRD Section 3.2.1.2.5.1.2a Poloidal Electrical Breaks]

##### Winding Tolerance

Background

The requirement for the installed coils is that the local current centroid of each Assembly shall be located within 1.5 mm of the nominal location defined in GRD Section A.1.1 Coil Centroids with the Assembly at the pre-pulse operating temperature with zero current. [Ref. SRD Section 3.2.1.2.5.4].  There are three major steps at which errors can be introduced: [1] coil manufacture; [2] field period assembly; and [3] final machine assembly.  In the absence of better knowledge, it was decided to apportion this tolerance equally for each step.

Requirement

The local current centroid of each Assembly shall be located within 0.5 mm of the nominal location defined in GRD Section A.1.1 Coil Centroids with the Assembly at the pre-pulse operating temperature with zero current.

#### Reference Scenario Requirements

Background

NCSX is designed to be a flexible, experimental test bed.  To ensure adequate dynamic flexibility, a series of reference scenarios has been established. TF, PF, and modular coil systems and the vacuum vessel will be designed for a plasma with a nominal major radius of 1.4 m and capability to meet the requirements of all the reference scenarios. Electrical power systems shall be designed and initially configured to meet the requirements of the First Plasma and Field Line Mapping Scenarios and shall be capable of being upgraded to meet the requirements of all other reference scenarios.

Reference scenario definitions are provided in Section 3.2.1.5.3.3.1 of the General Requirements Document.  Reference waveforms of engineering parameters such as coil currents, voltages, power dissipation, etc. are derived from the scenario specifications and are documented in GRD Appendix A.

Requirement

The Assembly will be designed to meet the requirements of all the reference scenarios.  [Ref. SRD Section 3.2.1.2.6.2 Reference Scenario Requirements]

#### Pulse Repetition Rate

Modular coils shall be designed for pulses to be initiated at intervals not exceeding 15 minutes when constrained by coil cooldown and 5 minutes otherwise.  [Ref. SRD Section 3.2.1.2.7 Pulse Repetition Rate]

#### Electrical Requirements

##### Electrical Isolation of the Conductor

The Assembly shall provide the following voltage standoff capability between the electrical circuit (conductor) and all other components outside the electrical circuit.

- Maximum Operating Voltage.  The maximum operating voltage is 2kV.

- Field Maintenance Test Voltage.  The field maintenance test voltage shall be twice the maximum operating voltage to ground plus 1 kV, i.e. 5kV.

- Manufacturing Test Voltage.  The manufacturing test voltage shall be 1.5 times the field maintenance test voltage, i.e. 7.5kV.

- Design Voltage Standoff.  The design voltage standoff shall be twice the manufacturing test voltage, i.e. 15kV.

##### Turn-to-turn Voltage Standoff

The Assembly shall be designed to provide a design voltage standoff from one turn of conductor to any adjacent turn of conductor of 600V which is approximately thirty-six times the maximum turn-to-turn voltage of 16.7V.

##### Electrical Isolation and Grounding of Other Components

Electrical isolation and grounding requirements for components of the Assembly other than the conductor are listed below.  The resistance of the electrical isolation features (e.g. electrical breaks in the coolant tubes and Kapton sheets on the cladding) shall be greater than 10 MOhms when tested at 1 kVDC.  High resistance grounds shall have a resistance of 100 ohms (TBR).

- Winding form. The winding form is connected to a high resistance, single point ground.

- Clamps.  The production clamps are electrically connected to the winding form through their mechanical attachments and electrically isolated from all other components.  Pre-loads are applied to the winding pack through an insulating, G-11CR plate.

- Cladding.  The cladding is electrically connected to the chill plates and electrically isolated from all other components.

- Chill plates.  The chill plates are electrically connected to the cladding and coolant tubes and electrically isolated from all other components.

- Coolant tube.  Each coolant tube shall have an insulating break at the supply and return ends as shown in the loop labeled B in Figure 3-3.  For those loops which span the poloidal break in the winding form, an additional insulating break is required at the location of the poloidal break as shown in the loop labeled A in Figure 3-3.  Each electrically isolated coolant tube shall be electrically connected to the winding form through a high resistance ground that can be lifted to test the electrical isolation.  All insulating breaks and high resistance grounds shall be located outside the winding form in a region accessible for maintenance.

- Co-wound diagnostic loops.  The co-wound diagnostic loops are connected to a junction box and electrically isolated from all other components by shrink tubing.  In addition, all diagnostics and instrumentation leads shall be isolated via optical and/or magnetic (isolation transformer) means prior to exiting the cryostat. The isolation shall be rated to withstand a one minute AC hipot test at 20 kV AC rms.

Figure 3-3 Electrical isolation and grounding of coolant loops

##### Electrical Resistance

The electrical resistance of the modular coil assembly shall be between 9- and 12-milliohm at room temperature and 1- to 2-milliohm at 80K.  Verify all by test at room temperature and the first article by qualification testing at temperature in the Coil Test Facility.

### Physical Characteristics

#### Winding Form

The product specification, NCSX-CSPEC-141-03, and its associated drawings defines the winding form assembly and requirements for its fabrication.

#### Attachments

Threaded studs and other attachments are welded to the winding form in order to facilitate winding operations.  Some attachments are to be removed after winding in order prevent interference during field period assembly. Details and requirements are defined on the attachments and post-VPI assembly drawings.

#### Winding Packs

The winding pack assemblies, designated "Side-A" and "Side-B", are composed of conductor and ground insulation surrounded by an assembly of cladding and chill plates for cooling.  The winding pack assembly shall slip relative to the winding form and not be permanently bonded to it. Further requirements are as follows:

##### Cladding

The cladding is a segmented layer of copper that lies between the winding pack and the winding form. All cladding parts shall be free of burrs and sharp edges that might damage the conductor, and all surfaces shall be roughened to promote bonding during the vacuum-pressure impregnation process. The cladding shall not be permanently bonded to the winding form.

##### Chill Plates and Coolant Tubes

The chill plates are a segmented layer of copper that covers the outer surfaces of the winding pack. All chill plates shall be free of burrs and sharp edges that might damage the conductor, and all surfaces shall be roughened to promote bonding during the vacuum-pressure impregnation process. Tubes are attached to the chill plates by soldering to form ten closed cooling loops per coil assembly. Verify installation by inspection and test.

##### Conductor

The product specification, NCSX-CSPEC-142-03, defines the physical requirements for the conductor and turn insulation. Supplemental turn insulation is required where the conductor penetrates the ground insulation at the leads.  The supplemental insulation shall be composed of two half-lapped layers of 1-in wide x .007-in S2 glass and .75-in wide x .0065-in adhesive Kapton tape, for a total thickness of .041-in.

##### Ground Insulation

The ground insulation is composed of S2 glass and adhesive Kapton.  The total thickness of 0.0445-in is composed of three layers: 1) a butt-lapped layer of 0.007-in S2 glass, 2) a half-lapped layer consisting of 2-in wide x 0.007-in S2 glass and 1.5-in wide x 0.0065-in adhesive Kapton tape, and 3) a butt-lapped layer of the same composite.

##### Lead Blocks

As shown on the referenced assembly drawings, the conductor lead blocks shall be pre-assembled to the winding form in order to align the starting lead blocks.  All components shall be free of burrs and sharp edges that might damage the conductor, and all surfaces shall be roughened to promote bonding during the vacuum-pressure impregnation process. Verify by visual and dimensional inspection.

##### Terminal Assembly

The terminal assembly includes the crossover jumpers and terminal lugs, as defined in the referenced drawings.  All electrical contact surfaces shall be clean, and all bolted connections shall be torqued to specified values.  All demountable electrical connections shall be accessible for maintenance and have provisions which ensure adequate contact pressure over time, i.e. under repeated thermal and mechanical loading.

##### Clamps

The clamps are defined by subassembly drawings and feature adjustable, spring loaded pads that provide a preload of ~125 lbs to the top and side of each winding pack.  Verify installation, including location per the assembly drawings, by inspection.

##### Co-wound Diagnostic Loops

Diagnostic flux loops, composed of .032-in diameter mineral insulated wire, are located between the chill plates and VPI bag mold near the plasma facing surface of each winding pack.  Supplemental insulation composed of shrink tubing shall be provided where the wire enters/exits the mold.  A length of wire, approx 20-ft, shall be left outside the VPI envelope for routing to a junction box on the vacuum vessel.  The location of the installed loops shall be measured prior to vacuum pressure impregnation.

##### Instrumentation

Each modular coil assembly shall be equipped with thermocouples on the winding form and voltage taps at the leads.  The first article of each coil type shall be instrumented with RTDs and strain gages as shown on the referenced drawings.  Verify installation by inspection and test.

##### Bag Mold Assembly

The bag mold is composed of two layers of half-lapped, self-fusing gray silicone tape and painted with 2-part RTV-11 (white). The bag mold is sealed to the winding form using .25-in diameter copper tubing, which is to be removed after fabrication. A structural shell, composed of glass-epoxy paste that is cured at room temperature, shall be provided to restrain the bag mold during vacuum pressure impregnation (VPI). The shell is removed after VPI. Verify by inspection and test.

#### Weight

The maximum weight of a completed modular coil assembly shall not exceed 6500 lbs.

### System Quality Factors

#### Reliability, Availability, and Maintainability

Background

The overall objective is to provide a device with high operational availability, meaning that the number of plasma discharges achieved in a run period is a large percentage (greater than 75%) of the number planned after the initial shakedown and commissioning phases of the facility.  Bottoms-up reliability predictions are difficult to perform and have large uncertainties for first-of-a-kind experimental devices such as NCSX.  Therefore, quantitative RAM requirements on NCSX will be few.  Rather, NCSX will rather rely on sound engineering practice to assure high availability in NCSX, which has been the tried-and-true approach on similar scale fusion devices.  Sound engineering practices include:

- Applying design principles that promote reliability (e.g., employing an adequate factor of safety on mechanical and electrical stresses, avoiding unnecessary complexity, using proven design approaches and well characterized materials, etc.)

- Optimizing designs for reliability and maintainability through systematic evaluation of design options,

- Performing failure modes, effects and criticality analysis (FMECAs) for RAM design improvement and verification, and

- Employing peer reviews as a mechanism to enhance the design process.

The NCSX RAM Plan defines the processes that will be used by the Project to achieve a device with high availability.

Requirements

- The Assembly shall incorporate reliability and maintainability features in the design that are consistent with achieving a very high (greater than 99%) operational availability for each Assembly.

- Provisions for recovery shall be made for every credible failure mode in the Assembly.

- Provisions for lifting, e.g. lifting eyes, other sling attachment provisions, or equivalent provisions, shall be made in the design of the Assembly.

[Ref. SRD Section 3.2.3.1 Reliability, Availability, and Maintainability]

#### Design Life

- The Assembly shall have a design life of >10 years when operated per the reference scenarios in Section 3.2.1.9.

- The Assembly shall be designed for the following maximum number of pulses when operated per the reference scenarios defined in Section 3.2.1.9 and based on the factors for fatigue life specified in the NCSX Structural and Cryogenic Design Criteria Document:

- 100 per day;

- 13,000 per year; and

- 130,000 lifetime.

[Ref. SRD Section 3.2.3.2 Design Life]

### Transportability

The Assembly shall be transportable via overhead crane and forklift as required for testing in the Coil Test Facility (CTF) and for assembling into field periods in the Tokamak Fusion Test Reactor (TFTR) Test Cell.

### Interface Requirements

#### Vacuum Vessel System (WBS 12) Interface Requirements

Background

The vacuum vessel is physically supported from the modular coil shell for vertical (gravity and net electromagnetic loads) and lateral loads.  The vacuum vessel is thermally insulated to reduce heat leakage from the vacuum vessel to the modular coils.  The vacuum vessel port extensions penetrate the modular coil shell. During field period assembly, the modular coils must be able to be assembled over the vacuum vessel.

Requirements

The modular coil assembly shall provide sufficient interior clearance to install over the vacuum vessel with port extensions and insulation.  Minimum clearance is defined by post-VPI modular coil assembly drawings. Verify by dimensional inspection.

#### Conventional Coils (WBS 13) Interface Requirements

Background

The TF, PF, and trim coils are attached to the Coil Support Structures, which are in turn attached to the Modular Coils.  The conventional coils introduce electromagnetic loads on the modular coils and vice versa. During field period assembly, the TF coils must be able to be assembled over the modular coils.

Requirements

The modular coil assembly shall provide sufficient exterior clearance to be installed inside the TF coil subassembly.  Minimum clearance is defined by post-vpi modular coil assembly drawings. Verify by dimensional inspection.

#### Coil Support Structures (WBS 15) Interface Requirements

Background

The support structure is composed of structural plates above and below the modular coils. The upper plate supports the gravity and net electromagnetic loads from the upper PF ring coils, upper external trim coils, central solenoid assembly, and cryostat.  The upper plate also provides out-of-plane support for the TF coils.  These loads are transmitted through the modular coil shell to the lower plate along with gravity loads from the modular coils, vacuum vessel, and in-vessel components.  Gravity loads from the stellarator core are transmitted through the lower plate to the Base Support Structure.

Requirements

The modular coil assembly shall interface with the support structure through the winding form shelf feature at R=39- and 79-inch locations. Verify feature by dimensional inspection.

#### Liquid Nitrogen Distribution System (WBS 161)

Background

LN2 SUPPLY.  Liquid nitrogen for coil cooling is supplied from the Cryogenic Systems (WBS 62) to the LN2 Distribution System (WBS 161), which in turn supplies the liquid nitrogen to the individual modular coils.

Requirements

The modular coil assembly shall interface with LN2 distribution through 1-in diameter winding form openings at the top, bottom, and outboard midplane locations. Verify feature by dimensional inspection.

#### Electrical Power Systems (WBS 4)

Background

The current and voltage required to drive the modular coils is supplied from the Electrical Power Systems (WBS 4) to the Electrical Leads (WBS 162), which in turn supplies the direct current (DC) power to the individual modular coils. Electrical Power Systems (WBS 4) provide coil protection via parameters measured in the power supply circuitry based on parameters provided by Coil Protection System (WBS 163) activities.  Electrical Power Systems (WBS 4) also provides coil protection via permissives and trip signals provided by Central I&C (WBS 5) in response to the output from sensors included in the local I&C within the Modular Coil System (WBS 14).  Electrical Power Systems (WBS 4) are responsible for providing single point grounds for the modular coil winding forms.

Requirements

The modular coil assembly shall interface with power systems through winding form openings near the outboard midplane, including openings for the conductor leads to enter/exit the winding pack as well as features for mounting the crossover and terminal assembly hardware. Verify features by dimensional inspection.

#### Central I&C (WBS 5)

Background

Central I&C (WBS 5) is responsible for taking the output from the sensors (e.g. strain gauges, resistance temperature detectors, and thermocouples) provided in the local I&C in the Modular Coil System (WBS 14), processing those signals, displaying and storing the data, and providing permissives and trip signals for coil protection to Electrical Power Systems (WBS 4) in accordance with the coil protection logic and parameters specified by the Coil Protection Systems (WBS 163).

Requirement

The design of the Assembly shall meet the physical interface requirements as defined by the referenced drawings.

## Design and Construction

### Materials, Processes, and Parts

#### Production Drawings

The Assembly shall be fabricated in accordance with the models and drawings listed in Section 5.1.

#### Magnetic Permeability

The Assembly shall have a relative magnetic permeability less than 1.02 unless otherwise authorized by the Project.  [Ref. SRD Section 3.3.1.1 Magnetic Permeability]

#### Corrosion Prevention and Control

Materials, processes, and protective surface treatments or finishes shall be provided to ensure that equipment capability during its service life is not degraded due to corrosion.  Where possible, contact between dissimilar metals shall be avoided.  [Ref. SRD Section 3.3.1.2 Corrosion Prevention and Control]

#### Flammable Materials

The use of flammable materials shall be minimized.  [Ref. SRD Section 3.3.6.3 Flammability]

#### Metrology

The Assembly shall provide features (e.g., fiducial markers) as required to facilitate accurately measuring and locating components relative to the magnetic field for the life of the machine.  [Ref. SRD Section 3.3.1.3 Metrology]

### Labels

Background

Equipment and any parts of that equipment to be used by personnel shall be identified with appropriate labels.  Labels shall indicate clearly and concisely the function and purpose of the item being labeled.  Hierarchical labeling shall be used to facilitate component location on control panels.  The terminology used for equipment, procedures, and training materials shall be the same for each case.  Label design shall be consistent to promote simplicity and avoid clutter.  The use of abbreviations and acronyms shall be minimized.  Permanent labels shall be attached to the specific component or equipment in such a manner that environmental conditions or usage by personnel will not remove or destroy the label.  Temporary labels shall be used only when necessary and shall not obscure other information or equipment.  If a temporary label is to designate a device that is out of service, the label shall be applied so that it prevents the use of that device.  Labeling shall be legible and conform to human visual capabilities and limitations in regard to physical characteristics.  [Ref. SRD Section 3.3.3.1 Labels]

Requirement

- The Assembly shall have a permanent label with the following minimum information – the name of the item and the part and serial number of the item, e.g. NCSX Modular Coil Type C Assembly, P/N SE140-103, S/N 1.  The label shall be located to be most easily viewed by maintenance personnel.

- Component parts of the Assembly shall be appropriately labeled.

### Workmanship

During Assembly fabrication and finishing, particular attention shall be given to freedom from blemishes, defects, burrs, and sharp edges; accuracy of dimensioning radii of weld fillets; making of parts; thoroughness of cleaning; quality of brazing, welding, riveting, painting, and wiring; alignment of parts; and tightness and torquing of fasteners.  [Ref. SRD Section 3.3.4 Workmanship]

### Interchangeability

Design tolerances shall permit Assemblies of the same part number to be used as replacement parts without degrading the specified performance of the parent item.  [Ref. SRD Section 3.3.5 Interchangeability]

# Quality Assurance Provisions

## General

The Assembly will be fabricated at PPPL in the Coil Manufacturing Facility (CMF) located in the TFTR Test Cell.  The design of the Assembly will be qualified by testing the first article at high current in the Coil Test Facility (CTF) to the extent practical.  Acceptance testing of subsequent articles will be performed in the CMF at the conclusion of Assembly fabrication.

The Project has sole responsibility for inspections and tests.  The Manager of the CMF has responsibility for those inspections and tests performed in the CMF.  The Manager of the CTF has responsibility for inspections and tests performed in the CTF.

## Verification Methods

Verification of qualification shall be by analysis, demonstration, inspection, or test.  Definition of analysis, demonstration, inspection, and test is as follows:

Analysis:  Verification of conformance with required characteristics by calculation or simulation, including computer modeling based on established material or component characteristics.

Inspection:  Verification of conformance by measuring, examining, testing, and gauging one or more characteristics of a product or service and comparing the results with specified requirements.

Test:  Verification by physically exercising a component or system under appropriate loads or simulated operating conditions, including measurement and analysis of performance data.

## Quality Conformance

This section establishes the specific methods for verification of requirements in Section 3.

### Verification of Design Verification Requirement

Verification of conformance with the design verification requirement (Section 3.2.1.1) shall be by inspection of the design to be accomplished during Final Design of the Assembly.

#### Verification of Coil Cool-down and Warm-up Timelines

Verification of conformance with the timeline requirements for coil cool-down (Section 3.2.1.2) and warm-up (Section 3.2.1.3) shall be by qualification testing in the Coil Test Facility for the first article.

#### Verification of Cool-down and Warm-up Cycles

Verification of conformance with the requirement for the number of cool-down and warm-up cycles specified in Section 3.2.1.4 shall be by analysis performed during Final Design.

#### Verification of Coil Temperatures during Bakeout

Verification of conformance with the coil temperatures during bakeout requirement in Section 3.2.1.5 shall be by analysis performed during Final Design.

#### Verification of Bakeout Cycles

Verification of conformance with the bakeout cycles requirement in Section 3.2.1.6 shall be by analysis performed during Final Design.

#### Verification of Pre-Pulse Temperature

Verification of conformance with the pre-pulse temperature requirement in Section 3.2.1.7 shall be [1] by analysis performed during Final Design and [2] by qualification testing in the Coil Test Facility for the first article.

#### Verification of Field Error Requirements

##### Verification of the Poloidal Electrical Breaks

Verification of conformance with the poloidal electrical break resistance requirement in Section 3.2.1.8.1 shall be by [1] acceptance testing each completed modular coil winding form at the Supplier and [2] acceptance testing of each completed Assembly in the Coil Manufacturing Facility.

##### Verification of Electrical Isolation

Verification of conformance with the electrical isolation requirement in Section 3.2.1.11.3 shall be by testing during coil manufacture.  Testing shall be performed at the earliest steps practical and again on the completed Assembly (where practical).

##### Verification of Winding Tolerance

- Verification of conformance with the winding tolerance requirement in Section 3.2.1.8.2 shall be by done by in-process inspection upon completion of coil winding.  The location of the local current centroid will be inferred from measurements of the winding form surface prior to winding and measurements of the conductor surface upon completion of winding.  The winding clamps will be used to move the location of the local current centroid to within the winding tolerance requirement.  Fiberglass straps will be used to stabilize the winding pack. The torque values required to set the winding clamps in the proper position shall be recorded and used to re-set the winding clamps each time they are removed.  This procedure shall be used to maintain the location of the local current centroid within the winding tolerance requirement for the remainder of Assembly fabrication.

- During acceptance testing of the completed Assembly, magnetic measurements shall be taken to reconstruct the location of the local current centroid and verify conformance with the winding tolerance requirement in Section 3.2.1.8.2.

#### Verification of Reference Scenario Requirements

- Verification of conformance with the reference scenario requirements in Section 3.2.1.9 shall be by analysis during Final Design.

- During qualification testing in the Coil Test Facility on the first article, key performance parameters (stresses, deflections, temperatures, pressures, etc.) shall be measured and compared to calculated values to assure that the Assembly is performing consistent with expectations, i.e. analysis.

#### Verification of Pulse Repetition Rate

Verification of conformance with the pulse repetition rate requirement in Section 3.2.1.10 shall be [1] by analysis during Final Design and [2] by qualification testing of the first article in the Coil Test Facility.

#### Verification of Electrical Requirements

##### Verification of Electrical Isolation of the Conductor

Verification of conformance with the electrical isolation requirements in Section 3.2.1.11.1 shall be accomplished as follows.

- Verification of Design Voltage Standoff.  The insulation system shall be qualified to the design voltage standoff (15kV) by testing during Final Design.

- Verification of Manufacturing Test Voltage.  Each Assembly shall be meggar tested at room temperature to the manufacturing test voltage (7.5kV) during acceptance testing in the Coil Manufacturing Facility.  In addition, the first article shall be meggar tested at cryogenic temperature to the manufacturing test voltage (7.5kV) during qualification testing in the Coil Test Facility.

##### Verification of Electrical Isolation and Grounding of Other Components

Verification of conformance with electrical isolation and grounding requirements in Section 3.2.1.11.3 shall be by [1] in-process tests during Assembly manufacture and [2] acceptance testing of the completed Assembly.  In addition, electrical isolation features shall be qualified during Final Design.  Specifically, the design of the electrical breaks in the coolant tubes shall be qualified by testing under representative conditions.

##### Verification of Electrical Resistance

Verification of conformance with the Electrical Resistance requirements in Section 3.2.1.11.4 shall be accomplished as follows:

- The electrical resistance of each Assembly (terminal-to-terminal) shall be measured at room temperature (20ºC) during acceptance testing in the Coil Manufacturing Facility.

- The electrical resistance of the first article (terminal-to-terminal) will be measured at cryogenic temperature (80K) during qualification testing in the Coil Test Facility.

### Verification of Physical Characteristics

#### Winding Form

Verification of conformance with the winding form specification requirements in Section 3.2.2.1 shall be accomplished by adherence to the quality assurance provisions of said specification.

#### Attachments

Verification of conformance with the attachments requirements in Section 3.2.2.2 shall be accomplished by dimensional inspection per the associated drawings.

#### Winding Packs

Verification of conformance with the winding pack requirements in Section 3.2.2.3 shall be accomplished by dimensional inspection per the associated drawings.

#### Cladding

Verification of conformance with the cladding requirements in Section 3.2.2.3.1 shall be accomplished by test of any temporary bonding and visual inspection per the associated drawings.

#### Chill Plates and Tubes

Verification of conformance with the chill plate and tube requirements in Section 3.2.2.3.2 shall be accomplished by test of any temporary bonding and visual inspection per the associated drawings.

#### Conductor

Verification of conformance with the conductor specification requirements in Section 3.2.2.3.3 shall be accomplished by adherence to the quality assurance provisions of said specification.

#### Ground Insulation

Verification of conformance with the ground insulation requirements in Section 3.2.2.3.4 shall be accomplished by electrical test and visual inspection.

#### Lead Blocks

Verification of conformance with the lead blocks assembly requirements in Section 3.2.2.3.5 shall be accomplished by dimensional inspection per the associated drawings.

#### Terminal Assembly

Verification of conformance with the terminal assembly requirements in Section 3.2.2.3.6 shall be accomplished by electrical test and visual inspection per the associated drawings.

#### Clamps

Verification of conformance with the clamp assembly requirements in Section 3.2.2.3.7 shall be accomplished by visual inspection per the associated drawings.

#### Diagnostic Loops

Verification of conformance with the diagnostic loops requirements in Section 3.2.2.3.8 shall be accomplished by electrical test and visual inspection per the associated drawings.

#### Instrumentation

Verification of conformance with the instrumentation requirements in Section 3.2.2.3.9 shall be accomplished by electrical test and visual inspection per the associated drawings.

#### Bag Mold Assembly

Verification of conformance with the bag mold requirements in Section 3.2.2.3.10 shall be accomplished by test and visual inspection per the associated drawings.

#### Weight

Verification of conformance with the weight requirements in Section 3.2.2.4 shall be accomplished by test.

### Verification of System Quality Factors

#### Reliability, Availability, and Maintainability

Verification of conformance with the reliability, availability, and maintainability requirements in Section 3.2.3.1 shall be accomplished by qualification testing of the first article of each coil type in the Coil Test Facility.

#### Design Life

Verification of conformance with the design life requirements in Section 3.2.3.2 shall be accomplished by analysis and test.

#### Transportability

Verification of conformance with the transportability requirements in Section 3.2.4 shall be accomplished by test.

### Verification of Interface Requirements

#### Vacuum Vessel

Verification of conformance with the vacuum vessel interface requirements in Section 3.2.5.1 shall be accomplished by dimensional inspection per the associated drawings.

#### Conventional Coils

Verification of conformance with the conventional coils interface requirements in Section 3.2.5.2 shall be accomplished by dimensional inspection per the associated drawings.

#### Coil Support Structures

Verification of conformance with the support structure interface requirements in Section 3.2.5.3 shall be accomplished by dimensional inspection per the associated drawings.

#### Liquid Nitrogen Distribution System

Verification of conformance with the LN2 supply interface requirements in Section 3.2.5.4 shall be accomplished by dimensional inspection per the associated drawings.

#### Electrical Power Systems

Verification of conformance with the power systems interface requirements in Section 3.2.5.5 shall be accomplished by dimensional inspection per the associated drawings.

#### Central I&C

Verification of conformance with the I&C interface requirements in Section 3.2.5.6 shall be accomplished by dimensional inspection per the associated drawings.

# Appendices

## Assembly Models and Drawings

### Modular Coil Assembly Type-A

Drawings to be provided

### Modular Coil Assembly Type-B

Drawings to be provided

### Modular Coil Assembly Type-C

# Text boxes

Controlled Document

This is a controlled document.  Check the NCSX Engineering Web prior to use to assure that this document is current.